Request Title:  Use of Lift off Resist PMGI SF 9

Requestor: 	Ludwig Galambos						Date:  12/10/2021

Non-SNF staff, please complete the following:

Badger ID: ludwig.galambos@gmail.com

Company name/PI: Novasolix

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. Please provide all common names, trade names, and CAS numbers where appropriate.

PMGI SF 9

Read the MSDSs as well as the Stanford Chemical Storage Groups to determine the Storage Group Identifier and Main Hazard Class of your chemical/material.

MSDS database on EH&S: https://chemtracker.stanford.edu/CTv1/servlet/chemsafe.detail?sunum=25162

GDN: 25162

Classification system:

ꞏ NFPA ratings (scale 0 - 4)

Health = 2

Fire = 3

Reactivity = 0

ꞏ HMIS-ratings (scale 0 - 4)

Health = 2

Fire = 3

Reactivity = 0

- Vendor/manufacturer info:

Kayaku Advanced Materials, Inc., 200 Flanders Road Westborough MA 01581

Tel: 617-965-5511

https://kayakuam.com/

- Reason for request:  For thick layer liftoff processing

- Process Flow - highlight steps use the PMGI SF 9

prime	vapor prime wafers, standard process			Yes oven

coat1	PMGI SF 9, 60s (~1000nm) recipe for SF 9			headway

bake	PMGI SF 9  bake 160-210 °C for 5 min			litho hotplate

coat2	Coat, 3612 resist, 1.0 µm, no vp, no EBR			svgcoat

clean	Dump rinse, SRD						SRD

expose	Exposure using ASML						ASML

develop	Std process for 3612 resist 1 µm,  postdevelop bake + develop 	svgdev

descum	Descum, O2 ~27 sccm, 50W for 60 s				Technics

deposit	Evaporation of metal layers					AJA-Evap

clean	Dump rinse, SRD						SRD

liftoff									wbflexsolv

1. Soak wafers in Remover PG at 60 °C for 30-60 min.

2. Pour warm 1165 solution to a small dish and move one wafer to the small dish.

3. Rinse wafers with fresh Remover PG.

4. Use acetone squeeze bottle to spray off loose metals on the wafer from the old 1165 bath

5. Put wafers in the warm Remover PG.

6. Ultrasonic wafer in Remover PG at 60°C for 1-3 min.

7. Use acetone squeeze bottom to spray on the patterns at a shallow angle, scan through the whole wafer and apply along 4 different directions,

8. Place wafer in acetone bath, sonicate at low power for 3 x 45-60 secs + acetone squeeze bottom spray.

9. Rinse with Acetone, Methanol, then with IPA, blow dry

10. Dump the waste Remover PG and acetone in the sbflexsolv waste solvent drain.

clean	dump rinse, SRD 						SRD

inspect	optical inspect							optical microscope

- Amount and form.
Q: How much will you bring in? (Note: as a general rule, powders are not permitted in the cleanroom.)
A: 500mL, liquid, in a bottle. 
Q: Do you need to mix it to use it?
A: No.

- Storage: Will you be storing your chemical/material at SNF?
Yes. We will label the bottle and storage it in the yellow cabinet right next to headway2.

Storage group: L (flammables and combustibles, including solvents)

- Disposal: How will you dispose of any waste or excess chemical or material? In your discussions with experts and vendors, try to determine the best way to dispose of your spent chemicals and by-products.
A: We have discussed the process with SNSF staff members as PMGI SF5 is a standard chemical in the SNSF nano-patterning lab.  We would use small amounts of material such that dumping the waste in the standard solvent waste carboy in wbflexsolv would be appropriate, similar to what SNSF does with this resist.

Please refer to the SNF Lab members Safety Manual for the different methods of waste disposal that are available in the lab.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: