Request Title:  Silicon etching in existing SPTS uetch vapor etcher

Requestor: 	Donald Gardner					Date:  9/21/2021

Non-SNF staff, please complete the following:

Badger ID:	don.gardner

Company name/PI: SLAC

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material.

  - Request to add compressed dry air (CDA) that is particle free to the uetch.

- Vendor/manufacturer info:

  - SPTS uetch vapor etch

- Reason for request:

- We want to etch high aspect ratio patterns into silicon.  This can be done using platinum as a catalyst that has been patterned on silicon (see reference [1] at https://doi.org/10.1039/C9NH00709A )

- CDA is needed for the process.  The CDA is already dried and has particle filters on it.  The proposal is to connect a two way valve to the gas inlet to the tool that allows the user to choose between either 100% nitrogen gas or compressed dry air.

- The uetch consists of a single chamber that is opened to atmosphere for loading and unloading samples, so there are no concerns for vacuum degradation by using CDA.

- Process Flow:

- Wafers are prepared with patterned platinum films deposited directly onto the silicon surface.  No photoresist is present on the wafers.

- The wafers are cut into smaller pieces and placed onto a carrier wafer that is placed into the substrate holder in the chamber.

- The uetch system has recipes that introduce HF vapor and nitrogen as part of the process.  CDA would be substituted for the nitrogen which would allow for the introduction of oxygen that can react with the silicon surface.

- Initially, the existing recipes will be utilized to examine the etch rates using the various HF vapor concentrations.

- The platinum metal acts as a catalyst. Silicon dissolution can occur via oxidation of Si and subsequent dissolution of SiO2 in the vapor HF:

  - Si + 2H2O → SiO2 + 4H+ + 4e−

  - SiO2 + 6HF → H2SiF6 + 2H2O

- Subsequently, possible optimization of the recipe would be considered and reviewed with Gary Yama, the tool owner depending on the results.

- Amount and form.

  - Silicon wafers with platinum films as needed.

  - Compressed dry air as needed.

  - Anhydrous HF that is already on the system.

- Storage:

  - No storage needed.

- Disposal:

  - Nothing to dispose of beyond what is already done with the existing system.

1.	Romano, L., et al., Metal assisted chemical etching of silicon in the gas phase: a nanofabrication platform for X-ray optics. Nanoscale Horizons, 2020. 5(5): p. 869-879.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: