Request Title: Preparing liquid crystal cell in SNF flexible clean room

Requestor: Anqi Ji					Date: Jul. 13rd, 2021

Non-SNF staff, please complete the following:

Badger ID: anqi@stanford.edu

Company name/PI: Stanford University/Prof. Mark L. Brongersma

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. 4′-Pentyl-4-biphenylcarbonitrile (5CB) liquid crystal 98%

- Vendor/manufacturer info: Sigma Aldrich

- Reason for request: We are testing a liquid crystal alignment method which uses oxygen plasma. For fulfill this purpose, we need to prepare a liquid crystal cell in the SNF flexible clean room.

- Process Flow:

- Treat one glass slide (G1) with ozone for 10 min.

- Drop nanosphere spacers on a second glass slide (G2).

- Put the two glass slides (G1 and G2) together with the nanospheres in between. Rotate and press the glass slide to spread out the nanospheres uniformly. Dry both slides using nitrogen gun. The nanospheres are dissolved in solution. (See the other prom request)

- Place glue on 4 corners of G2. Then place and press G1 onto G2 so the two can bond together to form a cell. Wait for the glue to dry.

- Use the pipette to drop the liquid crystal (5CB) near the gap. The liquid crystal should naturally fill the gap due to gravity and caterpillar force.

- Use cross-polarized microscopy to check the alignment.

- Amount and form. 1 gram, nematic liquid crystal.

- Storage: No.

- Disposal: Standard solvent waste

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: