Request Title:  SU-8 2100 photoresist

Requestor: Junyoung Hwang						Date:  11/15/2021

Non-SNF staff, please complete the following:

Badger ID: junhwang

Company name/PI: Stanford University/Ilenia Battiato

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. Please provide all common names, trade names, and CAS numbers where appropriate. Include an MSDS, if available; or provide the reason, if not. Make sure to include information for any new secondary chemicals (such as a developer for a new resist). Read the MSDSs as well as the Stanford Chemical Storage Groups to determine the Storage Group Identifier and Main Hazard Class of your chemical/material.

SU-8 2100 Permanent Epoxy Negative Photoresist

Ingredients: cyclopentanone (CAS: 120-92-3); mixed triarylsulfonium/ hexafluoroantimonate salt (CAS: 89452-37-9/CAS: 71449-78-0); propylene carbonate (CAS: 108-32-7); epoxy resin (CAS: 28906-96-9)

MSDS attached (‘SU8_MSDS.pdf’)

SU-8 developer will also be used and is available in the cleanroom.

- Vendor/manufacturer info: address and phone number, website URL.

Kayaku Advanced Materials, Inc.

200 Flanders Road

Westborough MA 01581

www.kayakuAM.com

Phone (617) 965-5511

Fax (617) 831-2354

- Reason for request: Please give serious thought to this. If you have any process information (application notes from the vendor, protocol from another lab, experimental methods section of an article), please include it, preferably as attachments. Ask yourself these questions: Is this the latest procedure? Are there newer/safer alternatives that will also work for my project? Will any of the current SNF approved chemicals and materials work for me?

The chemical will be used coat 4 inch silicon wafers to build PDMS molds with structures that are 50-200 µm tall. The coating process (spin speed/time, exposure time, bake conditions, etc.)  has been done before by a previous member of the group and has been documented for varying thicknesses. A publication that details the process is attached (‘Ling_energies_2020.pdf’)

- Process Flow: Please provide a detailed process flow description on how and where you proposed to use this chemical. This should include all Lab equipment to be used for processing your wafers once your new chemical or material has been used (even if your new material is a film that is removed, it may still pose potential contamination concerns.) Make sure to include wet benches. Please note that f the chemical/material is to be used in any the "clean" equipment, purity specifications will be needed. This is most important for chemicals/material that are not normally used for VLSI device fabrication. To be allowed into a "clean" tool, the material should MOS grade or better.

Process for coating SU-8 2100

- Dehydrate a silicon wafer and coat with HDMS (SNF equipment: YES oven)

- Spin coat the wafer (SNF equipment: Headway)

- Perform soft bake at two temperatures: 65 °C and 95 °C for (SNF equipment: hot plates)

- Expose the wafer with a chrome photomask (SNF equipment: Karl Suss MA-6)

- Perform post-exposure bake at 65 °C and 95 °C (SNF equipment: hot plates)

- Develop the coated wafer using SU-8 developer (SNF equipment: solvent bench in the litho area)

- Perform hard bake at 180 °C (SNF equipment: hot plates)

- Amount and form. How much will you bring in? Is it solid, powder or liquid? (Note: as a general rule, powders are not permitted in the cleanroom.) Do you need to mix it to use it?

Liquid 500 mL

- Storage: Will you be storing your chemical/material at SNF? If so, please note any potential reactivity’s (this should be on the MSDS). Storage groups A, B, D and L are stored in the yellow solvent cabinet in the furnace support area, while storage groups C, E, F and G are stored on top of one of the Pass-through Carts. Ensure your chemical container or material is properly labeled. If there is no available room, it must be stored by in the bulk storage area. You will then need to obtain it from receiving area personnel each time you want to use it and return it to them when you are finished using it (or each time you leave the lab). Note that there is no storage of chemicals/materials in the processing lab or at any wet bench.

The chemical will be stored in the cleanroom Headway cabinet designated for photoresist storage.

- Disposal: How will you dispose of any waste or excess chemical or material? In your discussions with experts and vendors, try to determine the best way to dispose of your spent chemicals and by-products. Please refer to the SNF Lab members Safety Manual for the different methods of waste disposal that are available in the lab.

Excess SU-8 resist will be disposed in the waste bin next to Headway bench.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: