Request Title:  Use of OmniCoat

Requestor: Yifan Kong					Date:  10/22/2021

Non-SNF staff, please complete the following:

Badger ID: yifank@science.xyz

Company name/PI: Science Corporation / Yifan Kong

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. Please provide all common names, trade names, and CAS numbers where appropriate. Include an MSDS, if available; or provide the reason, if not. Make sure to include information for any new secondary chemicals (such as a developer for a new resist). Read the MSDSs as well as the Stanford Chemical Storage Groups to determine the Storage Group Identifier and Main Hazard Class of your chemical/material.

OmniCoat

MSDS is attached

Developer is not necessary – O2 plasma to dessum or wet strip in NMP

- Vendor/manufacturer info: address and phone number, website URL.

Kayaku Advanced Materials

200 Flanders Road

Westborough, MA 01581 USA

Tel: 617-965-5511

https://kayakuam.com/products/omnicoat/

- Reason for request: Please give serious thought to this. If you have any process information (application notes from the vendor, protocol from another lab, experimental methods section of an article), please include it, preferably as attachments. Ask yourself these questions: Is this the latest procedure? Are there newer/safer alternatives that will also work for my project? Will any of the current SNF approved chemicals and materials work for me?

Sacrificial layer and adhesion promotor for SU-8. I wish to bring it in for personal use. Will use for liftoff of SU-8.

- Process Flow: Please provide a detailed process flow description on how and where you proposed to use this chemical. This should include all Lab equipment to be used for processing your wafers once your new chemical or material has been used (even if your new material is a film that is removed, it may still pose potential contamination concerns.) Make sure to include wet benches. Please note that f the chemical/material is to be used in any the "clean" equipment, purity specifications will be needed. This is most important for chemicals/material that are not normally used for VLSI device fabrication. To be allowed into a "clean" tool, the material should MOS grade or better.

I will be using Omnicoat as an underlayer for SU8, so that the SU-8 structures may be lifted off. I will spin Omnicoat on 4” wafers using Laurell spinner, then bake at 200C for 1 min. After this I will spin SU-8 on top of the wafer on Laurell spinner again, followed by soft bake on hotplate for ~1 hour and then expose on Karlsuss and develop on solvent bench. I will take the structure out of the SNF for final stripping of omnicoat.

- Amount and form. How much will you bring in? Is it solid, powder or liquid? (Note: as a general rule, powders are not permitted in the cleanroom.) Do you need to mix it to use it?

I will bring 100mL of omnicoat. No mixing required.

- Storage: Will you be storing your chemical/material at SNF? If so, please note any potential reactivity’s (this should be on the MSDS). Storage groups A, B, D and L are stored in the yellow solvent cabinet in the furnace support area, while storage groups C, E, F and G are stored on top of one of the Pass-through Carts. Ensure your chemical container or material is properly labeled. If there is no available room, it must be stored by in the bulk storage area. You will then need to obtain it from receiving area personnel each time you want to use it and return it to them when you are finished using it (or each time you leave the lab). Note that there is no storage of chemicals/materials in the processing lab or at any wet bench.

Yes, I will store it in the cleanroom. I will store it in the cabinet next to the SRD.

- Disposal: How will you dispose of any waste or excess chemical or material? In your discussions with experts and vendors, try to determine the best way to dispose of your spent chemicals and by-products. Please refer to the SNF Lab members Safety Manual for the different methods of waste disposal that are available in the lab.

Excess waste will be deposited in solvent contaminated waste bins – contaminated wipes, foil, and gloves will be put in a plastic bag and disposed of in the bins.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: