Request Title:  PCz/toluene mixture for Carbon Nanotube coating of wafers

Requestor: 	Nate Safron					Date:  11/21/2021

Non-SNF staff, please complete the following:

Badger ID:	nsafron@tsmc.com

Company name/PI: TSMC

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. Please provide all common names, trade names, and CAS numbers where appropriate. Include an MSDS, if available; or provide the reason, if not. Make sure to include information for any new secondary chemicals (such as a developer for a new resist). Read the MSDSs as well as the Stanford Chemical Storage Groups to determine the Storage Group Identifier and Main Hazard Class of your chemical/material.

- Vendor/manufacturer info: address and phone number, website URL.

- Reason for request: Please give serious thought to this. If you have any process information (application notes from the vendor, protocol from another lab, experimental methods section of an article), please include it, preferably as attachments. Ask yourself these questions: Is this the latest procedure? Are there newer/safer alternatives that will also work for my project? Will any of the current SNF approved chemicals and materials work for me?

- Process Flow: Please provide a detailed process flow description on how and where you proposed to use this chemical. This should include all Lab equipment to be used for processing your wafers once your new chemical or material has been used (even if your new material is a film that is removed, it may still pose potential contamination concerns.) Make sure to include wet benches. Please note that f the chemical/material is to be used in any the "clean" equipment, purity specifications will be needed. This is most important for chemicals/material that are not normally used for VLSI device fabrication. To be allowed into a "clean" tool, the material should MOS grade or better.

- Amount and form. How much will you bring in? Is it solid, powder or liquid? (Note: as a general rule, powders are not permitted in the cleanroom.) Do you need to mix it to use it?

- Storage: Will you be storing your chemical/material at SNF? If so, please note any potential reactivity’s (this should be on the MSDS). Storage groups A, B, D and L are stored in the yellow solvent cabinet in the furnace support area, while storage groups C, E, F and G are stored on top of one of the Pass-through Carts. Ensure your chemical container or material is properly labeled. If there is no available room, it must be stored by in the bulk storage area. You will then need to obtain it from receiving area personnel each time you want to use it and return it to them when you are finished using it (or each time you leave the lab). Note that there is no storage of chemicals/materials in the processing lab or at any wet bench.

- Disposal: How will you dispose of any waste or excess chemical or material? In your discussions with experts and vendors, try to determine the best way to dispose of your spent chemicals and by-products. Please refer to the SNF Lab members Safety Manual for the different methods of waste disposal that are available in the lab.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date:

  - We want to use:

    - poly[9-(1-octylonoyl)-9H-carbazole-2,7-diyl] (PCz) which is extremely similar to poly(9,9-di-n-dodecylfluorene) (PFD), CAS# 248256-53-3

    - carbon nanotubes, CAS# 308068-56-6

    - toluene, CAS# 108-88-3

The prepared PCz-nanotube-toluene solution will be brought into the SNFEXFAB. We do not have a SDS for the PCz, as it was custom manufactured for us. However since it is very similar to PFD polymer, we included the SDS for that polymer and additionally and SDS from commercially available PFD-nanotube-toluene solution to show that there are no additional hazards from the combination of materials

  - Material suppliers:

    - Toluene:	Sigma-Aldrich Inc.

3050 SPRUCE ST

ST. LOUIS MO 63103

Tel: (314) 771-5765

www.sigmaaldrich.com/

    - Carbon nanotubes:

Carbon Solutions, Inc.

1200 Columbia Ave.

Riverside, CA 92507

Tel: (951) 682-5620

carbonsolution.com

    - poly[9-(1-octylonoyl)-9H-carbazole-2,7-diyl] (PCz):

American Dye Source

555 Morgan Blvd

Baie-D'Urfe, Quebec H9X 3T6, Canada

Tel: +1 514-457-0070

https://adsdyes.com/

  - The purpose of these chemicals is to coat a wafer with a thin film of semiconducting carbon nanotubes. The PCz molecule wraps around preferentially semiconducting carbon nanotubes, making them soluble in toluene. This PCz-nanotube-toluene solution will be prepared outside SNF before bringing to the SNF EXFAB. Then in the SNF EXFAB, the nanotubes can be coated onto a wafer by soaking the wafer in the PCz-nanotube-toluene solution.

  - This process can be performed at the wet bench in Capitola, but a bath sonicator will need to be provided there. We confirmed with Michelle and Swaroop that an extra table-top sonicator is available. We would supply our own beakers. Nitrile gloves >.11 mm plus vinyl gloves and lab coat will be worn to avoid skin exposure.

    - First the CNT-polymer solution in Toluene is gently sonicated in a closed bottle.

    - Next, the wafer is coated by soaking the wafer in a beaker with the toluene-CNT-polymer solution for up to 12 hours. The beaker will be covered by aluminum foil and labeled with a blue tag.

    - After coating, the carbon nanotube wafers will be cleaned by rinsing in toluene.  Then it will be transfer to a fresh iso-propanol solution and dried in N2. A sub-monolayer of nanotubes will remain after the treatment.

    - Next, the sample would continue device fabrication through PVD (AJA evaporator or Lesker sputter), lithography (Headway, SVG Coat, Heidelberg, SVG Develop), ALD (Savannah or Fiji3), and/or etching (Oxford RIE). The nanotube layer is well-adhered to the substrate.

  - We will bring in:

    - Pre-mixed, concentrated PCz-nanotube-toluene solution ~ 50 mL.

    - Toluene ~ 1L bottle to dilute the CNT solution before deposition and rinse the wafer after deposition.

    - Then a wafer or piece of wafer.

  - We will need to store both the concentrated PCz-nanotube-toluene solution and pure toluene with Storage Group L (preferably in Mavericks). The toluene is the bulk component and is a combustible organic solvent, the main hazard class is flammable. The addition of the PCz and carbon nanotubes do not add any compatibility concerns for storage.

  - The PCz-nanotube-toluene solution and rinse toluene can be temporarily disposed into a marked waste container specific to these materials. This waste can be temporarily stored in Storage Group L. From the PFD-nanotube-toluene solution MSDS, solvent waste containing nanotubes and polymer can incinerated similarly to liquid solvent waste. Therefore, for waste collection, we believe this process waste can be mixed into the other liquid solvent waste carboy. If the liquid solvent waste is not typically incinerated, this process waste will need to be picked up for local collection.