Request Title: Polymer Diffraction Gratings for Ashing and ALD

Requestor: Baeddan Hill (Sr. Materials Engineer) 				Date:  9/22/2021

Non-SNF staff, please complete the following:

Badger ID: ajsnfconsult@gmail.com

Company name/PI: DigiLens, Inc./Michiel Callens

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. Polymer grating structures on glass substrates. We are not sure of the exact composition and do not have an MSDS, but expect a similar safety profile to other acrylate-based polymers. The samples are a composite of different acrylics and may show some degree of thermal degradation near or above 100°C. The diffraction efficiency of these gratings is highly sensitive to the physical dimensions and optical properties (i.e. refractive index) of the polymer. Thermal changes to the polymer (e.g. due to chemical reactions or outgassing) will likely present as changes in diffraction efficiency or peak shapes/angles. To evaluate the potential for thermal degradation we performed the following test:

  - Thin polymer gratings were cured overnight, then soaked in IPA and dried under nitrogen to remove any unreacted or volatile components, and finally ashed under an O2 plasma for 2 minutes to remove any weak or reactive components from the polymer. This is how the samples would be prepared prior to entering the ALD chamber.

  - The diffraction efficiency of the samples was measured. Then they were placed in an oven at 100°C for one hour, removed and allowed to cool, and remeasured. Minor changes were noticed in some cases, but were within the noise tolerance of the measurement apparatus. Therefore, we expect little to no change in the polymer structure or optical properties within this temperature range (i.e. below 100°C).

- Vendor/manufacturer info: N/A

- Reason for request: We would like to perform O2 ashing and ALD on these polymer grating structures.

- Process Flow: Samples will be first ashed in the Samco PC300 Plasma Etch System and then coated with AlOx and TiOx in the Savannah and/or Fiji ALD chambers. Samples are cleaned prior to ashing and, following ashing, should be thermally stable up to 100°C in the ALD chambers. If needed, samples could be pre-baked prior to ALD.

- Amount and form. Polymer films will be < 2 µm in thickness (0.3 – 1.0 µm is typical) on glass substrates.

- Storage: Samples will not be stored at SNF.

- Disposal: Samples will be returned to DigiLens and not disposed of at SNF.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: