Request Title:  BCB for wafer bonding, subsequent processing

Requestor: 	Chris Anderson						Date:  12/10/21

Non-SNF staff, please complete the following:

Badger ID:	cpa@stanford.edu

Company name/PI: Jelena Vuckovic

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. Please provide all common names, trade names, and CAS numbers where appropriate. Include an MSDS, if available; or provide the reason, if not. Make sure to include information for any new secondary chemicals (such as a developer for a new resist). Read the MSDSs as well as the Stanford Chemical Storage Groups to determine the Storage Group Identifier and Main Hazard Class of your chemical/material.

BCB, Benzocyclobutene, CycloteneTM

CAS: 694-87-1

MSDS attached

Hazard: Flammable

- Vendor/manufacturer info: address and phone number, website URL.

Sigma-Aldrich Inc.

3050 SPRUCE ST

ST. LOUIS MO 63103

UNITED STATES

+1 314 771-5765

https://www.sigmaaldrich.com/US/en/product/aldrich/164410

- Reason for request: Please give serious thought to this. If you have any process information (application notes from the vendor, protocol from another lab, experimental methods section of an article), please include it, preferably as attachments. Ask yourself these questions: Is this the latest procedure? Are there newer/safer alternatives that will also work for my project? Will any of the current SNF approved chemicals and materials work for me?

BCB is a standard adhesive polymer for low-temperature wafer bonding and heterogenous integration of electrical, mechanical and optical devices. Our lab needs to use this material to wafer bond various materials onto Si,SOI, Sapphire, SiC. Due to BCB’s high adhesive strength, low optical and microwave loss it a unique material that we require for our work.

- Process Flow: Please provide a detailed process flow description on how and where you proposed to use this chemical. This should include all Lab equipment to be used for processing your wafers once your new chemical or material has been used (even if your new material is a film that is removed, it may still pose potential contamination concerns.) Make sure to include wet benches. Please note that f the chemical/material is to be used in any the "clean" equipment, purity specifications will be needed. This is most important for chemicals/material that are not normally used for VLSI device fabrication. To be allowed into a "clean" tool, the material should MOS grade or better.

  - BCB spinning will be done outside SNF. Wafers will be bonded with BCB and cured at 250 C outside SNF.

  - In SNF, we will grind and polish our regular materials which are affixed to the carrier using the BCB adhesive. BCB will not be removed nor come in contact directly with tools.

  - Etching of our top layer material (bonded to the carrier by BCB) will occur in SNF using our normal recipes in OX-35, OX-RIE, PT-MTL. BCB does not need to be etched, though may unintentionally be etched. BCB is an organic polymer much like other resists and adhesives.

- Amount and form. How much will you bring in? Is it solid, powder or liquid? (Note: as a general rule, powders are not permitted in the cleanroom.) Do you need to mix it to use it?

We will only bring in the material that is spun in a micron scale layer on our films

- Storage: Will you be storing your chemical/material at SNF? If so, please note any potential reactivity’s (this should be on the MSDS). Storage groups A, B, D and L are stored in the yellow solvent cabinet in the furnace support area, while storage groups C, E, F and G are stored on top of one of the Pass-through Carts. Ensure your chemical container or material is properly labeled. If there is no available room, it must be stored by in the bulk storage area. You will then need to obtain it from receiving area personnel each time you want to use it and return it to them when you are finished using it (or each time you leave the lab). Note that there is no storage of chemicals/materials in the processing lab or at any wet bench.

Not stored in SNF

- Disposal: How will you dispose of any waste or excess chemical or material? In your discussions with experts and vendors, try to determine the best way to dispose of your spent chemicals and by-products. Please refer to the SNF Lab members Safety Manual for the different methods of waste disposal that are available in the lab.

N/A, this material will not be disposed of in SNF. Any contaminated chips will go in a solid waste bag.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: