Request Title:  Block Copolymer Etch in Lampoly

Requestor: Maryann Tung				Date:  April 4, 2021

Non-SNF staff, please complete the following:

Badger ID: tungmc

Company name/PI: H.-S. Philip Wong

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. Please provide all common names, trade names, and CAS numbers where appropriate. Include an MSDS, if available; or provide the reason, if not. Make sure to include information for any new secondary chemicals (such as a developer for a new resist). Read the MSDSs as well as the Stanford Chemical Storage Groups to determine the Storage Group Identifier and Main Hazard Class of your chemical/material.

The pieces to be etched are Si wafers (SNF stockroom) with 2 nm Ti / 35 nm Pt alignment marks and 30 nm TiN electrodes.  The whole piece will be covered by 30 nm SiO2 / 50 nm a-Si / 80 nm SiO2 and a very thin (<20 nm) block copolymer film.

- Vendor/manufacturer info: address and phone number, website URL.

The block copolymer film is the only component that is purchased from a vendor – the rest of the process is performed in-house.  The polymer was approved previously: https://docs.google.com/document/u/1/d/e/2PACX-1vRa2CMHzYEn9ZObM_dCYOfDshxCcGYqceKIxdQHFKIuE9lvu9HbGnHdIb7o_CHknFi-fy4siiUz1_L5/pub.

- Reason for request: Please give serious thought to this. If you have any process information (application notes from the vendor, protocol from another lab, experimental methods section of an article), please include it, preferably as attachments. Ask yourself these questions: Is this the latest procedure? Are there newer/safer alternatives that will also work for my project? Will any of the current SNF approved chemicals and materials work for me?

The block copolymer features are very small (CD = 20 nm) and require very precise etching with strong control over the sidewall angle.  So far, lampoly is the only tool in SNF that I have found that can successfully transfer the block copolymer patterns with good fidelity into the a-Si hardmask.

My request is to etch semi-clean wafers in lampoly, as my samples will have Ti/Pt alignment marks for processing in the JEOL e-beam lithography tool.  The alignment marks will not be etched in lampoly, as they will be covered by 30 nm SiO2 at minimum and therefore will not interact with the plasma.

- Process Flow: Please provide a detailed process flow description on how and where you proposed to use this chemical. This should include all Lab equipment to be used for processing your wafers once your new chemical or material has been used (even if your new material is a film that is removed, it may still pose potential contamination concerns.) Make sure to include wet benches. Please note that f the chemical/material is to be used in any the "clean" equipment, purity specifications will be needed. This is most important for chemicals/material that are not normally used for VLSI device fabrication. To be allowed into a "clean" tool, the material should MOS grade or better.

Starting with a silicon wafer from the SNF stockroom:

- Deposit 200 nm SiO2 (ccp-dep)

- Spin coat MMA/PMMA (SNSF solvent wet bench)

- Pattern in JEOL e-beam lithography tool (SNSF)

- Develop in 1:3 MIBK:IPA (SNSF solvent wet bench)

- Evaporate 2 nm Ti / 35 nm Pt (aja-evap)

- Lift off excess Ti/Pt in RemoverPG (solvent wet bench in Allen 213X)

- Deposit 30 nm TiN (AJA sputtering tool in Allen 111X)

- Spin coat and soft bake ma-N 2401 resist (SNSF solvent wetbench)

- Pattern in JEOL e-beam lithography tool (SNSF)

- Develop in MF 319 (SNSF base wetbench)

- Etch TiN (pt-mtl)

- Strip ma-N resist in O2 plasma (technics)

- Descum ma-N resist in SRS-100 (wbresstrip – flexible bath)

- Deposit 30 nm SiO2 / 50 nm a-Si / 80 nm SiO2 (ccp-dep)

- Spin and soft bake PMMA 950K A3 resist (SNSF solvent wetbench)

- Pattern in JEOL e-beam lithography tool (SNSF)

- Develop in 1:3 MIBK:IPA (SNSF solvent wetbench)

- Etch SiO2 (oxford-rie)

- Strip resist in acetone (lithosolv)

- Descum in O2 plasma (technics)

- Clean samples in SRS-100 (wbresstrip – flexible bath)

- Spin coat PS-b-PMMA block copolymer (headway3)

- Bake at 200 °C (white-oven)

- Expose in DUV lamp (Allen 213X lamp)

- Develop out PMMA in acetic acid (wbflexcorr)

- Etch remaining block copolymer (lampoly)

- Strip block copolymer (technics)

- Amount and form. How much will you bring in? Is it solid, powder or liquid? (Note: as a general rule, powders are not permitted in the cleanroom.) Do you need to mix it to use it?

One 1” x 1” piece will be etched per run.

- Storage: Will you be storing your chemical/material at SNF? If so, please note any potential reactivity’s (this should be on the MSDS). Storage groups A, B, D and L are stored in the yellow solvent cabinet in the furnace support area, while storage groups C, E, F and G are stored on top of one of the Pass-through Carts. Ensure your chemical container or material is properly labeled. If there is no available room, it must be stored by in the bulk storage area. You will then need to obtain it from receiving area personnel each time you want to use it and return it to them when you are finished using it (or each time you leave the lab). Note that there is no storage of chemicals/materials in the processing lab or at any wet bench.

Samples will not be stored in SNF.

- Disposal: How will you dispose of any waste or excess chemical or material? In your discussions with experts and vendors, try to determine the best way to dispose of your spent chemicals and by-products. Please refer to the SNF Lab members Safety Manual for the different methods of waste disposal that are available in the lab.

n/a

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: