Request Title: 	Use of Photoresist MIR701 in SNF

Requestor: Noriyuki Sato						Date:  4/15/2021

Non-SNF staff, please complete the following:

Badger ID: noriyuki@keplercompute.com

Company name/PI: Kepler Computing Inc. / Niloy Mukherjee

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. Positive photoresist MIR701. MSDS attached:

- Vendor/manufacturer info:

EMD Performance Materials Corp., An affiliate of Merck KGaA, Darmstadt Germany

One International Plaza, Suite 300, Philadelphia, PA 19113

1-888-367-3275

https://www.microchemicals.com/products/photoresists/az_mir_701.html

- Reason for request: Kepler Computing currently has a process baseline at UCB NL where we use MIR701. We would like to match process between NL and SNF as much as possible and therefore request approval for using MIR701.

- Process Flow:

- 4 inch Si or piece is spin-coated using Headway 2, soft bake at 90deg C.

- Exposure using Karl Suss MA-6 Contact Aligner 1/2

- Post bake at 115deg C

- Development using MF26A on Wet Bench Miscellaneous

- (Process continues in SNSF)

- Amount and form. 16 – 32 oz. It is liquid. We do not mix it to use it.

- Storage: Will be stored in SNF. Storage group is L.

- Disposal: The waste during spin-coating will be in zip-rock bag and disposed in resist-waste trash can.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: