Request Title: Etching / cleaning BTO and STO films in MRC etcher

Requestor: Yao-Te Cheng (PsiQ)					Date:  12/09/2021

Non-SNF staff, please complete the following:

Badger ID: ytcheng@stanford.edu

Company name/PI: PsiQ Corp/Chia-Ming Chang

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material.
BTO stands for BaTiO3 or barium titanate.  STO stands for SrTiO3 or strontium titanate.  Since these BTO and STO we use are films that were sputter deposited, we don’t have specific MSDS forms our film. But we can provide an MSDS of solid phase (not powder) barium titanate and strontium titanate from Materion as references.  In addition, Stanford EH&S MSDS database has BTO and STO.
BTO: https://chemtracker.stanford.edu/CTv1/servlet/chemsafe.detail?sunum=968
STO: https://chemtracker.stanford.edu/CTv1/servlet/chemsafe.detail?sunum=10490

Storage Group: G

- Vendor/manufacturer info:
Prefer not to disclose our third-party vendor.

- Reason for request: 
We would like to clean or etch our BTO and STO films, which was sputter deposited by our vendor on silicon in a UHV chamber.

- Process Flow: 
We intend to clean our BTO and STO films at SNF and investigate the surface roughness and uniformity after plasma cleaning in the MRC etcher and how this can affect our BTO and STO films.  We also intend to investigate the etching capability for our BTO and STO films.  While BTO and STO films will be deposited outside of SNF, we plan to perform the following steps at SNF:
(1) DI-water clean at wbflexcorr1-4 wet benches
(2) Solvent clean with acetone/methanol/IPA of our BTO and STO films at wbflexsolv.
(3) Cleaning or etching our BTO and STO films in MRC etcher using the available gases in MRC.
(4) Post-cleaning or post-etching inspection using one or any of the following SNF equipment: optical microscope, woollam, s-neox, filmetrics, stresstest, alphastep.
(5) (optional) PECVD or HDPCVD silicon oxide deposition on our BTO or STO films. (This process was previously approved by PROM committee.)

- Amount and form. 
BTO films are solid continuous layers deposited on 2-4” Si substrates/wafers, polycrystalline, 150-300nm thick, no powders.

- Storage: 
The BTO and STO films are on silicon substrates/wafers and will be storage on single wafer carriers.  The samples will be temporarily storage in the SNF storage bin during processing, but will, in general, not storage in SNF for a long term.
Storage group: G (not intrinsically reactive or flammable or combustible)

- Disposal: 
We do not expect to dispose our samples in SNF.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: