Request Title: Request for use of hydrogel-based photoresist (NIPAM)

Requestor: Paul Chong and Grace Woods				Date:  12APR2021

Non-SNF staff, please complete the following:

Badger ID: pxc, grawoods

Company name/PI: Guosong Hong

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material.

Please provide all common names, trade names, and CAS numbers where appropriate. Include an MSDS, if available; or provide the reason, if not. Make sure to include information for any new secondary chemicals (such as a developer for a new resist). Read the MSDSs as well as the Stanford Chemical Storage Groups to determine the Storage Group Identifier and Main Hazard Class of your chemical/material.

N,N’-methylenebisacrylamide

- CAS: 110-26-9

- Vendor: Sigma-Aldrich

- Amount: 100 g

- Hazards: toxic, sensitizer

- Storage group: G

N-isopropylacrylamide (NIPAm)

- CAS: 2210-25-5

- Vendor: Sigma-Aldrich

- Amount: 10 g

- Hazards: corrosive, acutely toxic (category 4)

- Storage group: G

lithium phenyl-2,4,6-trimethylbenzoylphosphinate

- CAS: 85073-19-4

- Vendor: Sigma-Aldrich

- Amount: 2x 1 g (2 g total)

- Hazards: not hazardous

- Storage group: G

diphenyl(2,4,6-trimethylbenzoyl)phosphine oxide

- CAS:75980-60-8

- Vendor: Sigma-Aldrich

- Amount: 10 g

- Hazards: acutely toxic (category 4), sensitizer, hazardous to environment

- Storage group: G

acrylic acid

- CAS: 79-10-7

- Vendor: Sigma-Aldrich

- Amount: 500 g

- Hazards: flammable, corrosive, acutely toxic (category 4), hazardous to environment

- Storage group: L, D

1-butanol (butyl alcohol)

- CAS: 71-36-3

- Vendor: Sigma-Aldrich

- Amount: 1 L

- Hazards: flammable, corrosive, acutely toxic (category 4)

- Storage group: L

1,2-ethanediol (ethylene glycol)

- CAS: 107-21-1

- Vendor: Sigma-Aldrich

- Amount: 1 L

- Hazards: sensitizer, acutely toxic (category 4)

- Storage group: G

1,2-propanediol (propylene glycol)

- CAS: 57-55-6

- Vendor: Sigma-Aldrich

- Amount: 500 mL

- Hazards: nonhazardous

- Storage group: G

1,2,3-propanetriol (glycerol)

- CAS: 56-81-5

- Vendor: Sigma-Aldrich

- Amount: 100 mL

- Hazards: nonhazardous

- Storage group: G

Chemicals will be used to develop new hydrogel-based photoresist for use in ENGR 241 in Spring 2021.

- Vendor/manufacturer info: address and phone number, website URL.

Vendor: Sigma-Aldrich

Sigma-Aldrich
Technical Services
PO Box 14508
St. Louis, MO 63178
UNITED STATES

Phone: 800-325-5832

Website URL: https://www.sigmaaldrich.com/united-states.html

- Reason for request: Please give serious thought to this. If you have any process information (application notes from the vendor, protocol from another lab, experimental methods section of an article), please include it, preferably as attachments. Ask yourself these questions: Is this the latest procedure? Are there newer/safer alternatives that will also work for my project? Will any of the current SNF approved chemicals and materials work for me?

Chemicals listed will be used to formulate a new stimuli-responsive hydrogel photoresist, which is currently being funded by ENGR 241. We plan on making the photoresist in our own lab and will bring it, in liquid form, into SNF.

References:

(1) 	Bassik, N.; Abebe, B. T.; Laflin, K. E.; Gracias, D. H. Photolithographically Patterned Smart Hydrogel Based Bilayer Actuators. Polymer (Guildf). 2010, 51 (26), 6093–6098. https://doi.org/10.1016/J.POLYMER.2010.10.035.

(2) 	Hippler, M.; Blasco, E.; Qu, J.; Tanaka, M.; Barner-Kowollik, C.; Wegener, M.; Bastmeyer, M. Controlling the Shape of 3D Microstructures by Temperature and Light. Nat. Commun. 2019, 10 (1), 1–8. https://doi.org/10.1038/s41467-018-08175-w.

- Process Flow: Please provide a detailed process flow description on how and where you proposed to use this chemical. This should include all Lab equipment to be used for processing your wafers once your new chemical or material has been used (even if your new material is a film that is removed, it may still pose potential contamination concerns.) Make sure to include wet benches. Please note that f the chemical/material is to be used in any the "clean" equipment, purity specifications will be needed. This is most important for chemicals/material that are not normally used for VLSI device fabrication. To be allowed into a "clean" tool, the material should MOS grade or better.

Chemicals will be used to formulate a new photoresist in house (Guosong Hong lab) outside of SNF and will be brought into SNF in a closed container. Resist will be spin coated (Headway) onto a film of SU-8 on a silicon wafer, edges will be wiped with a wetted foam spear-tipped applicator swab to remove edge bead and prevent resist from flowing off wafer, photopatterned with the Karlsuss and Heidelberg 1 or 2, and developed in DI water and/or isopropanol. This material poses little contamination risk, especially compared to SU-8 which already has a working protocol of use with the equipment listed.

- Amount and form. How much will you bring in? Is it solid, powder or liquid? (Note: as a general rule, powders are not permitted in the cleanroom.) Do you need to mix it to use it?

Chemicals will be used to formulate a new photoresist in house (Guosong Hong lab) outside of SNF and will be brought into SNF in a closed container (20-mL scintillation vial) in liquid form (< 20 mL).

- Storage: Will you be storing your chemical/material at SNF? If so, please note any potential reactivity’s (this should be on the MSDS). Storage groups A, B, D and L are stored in the yellow solvent cabinet in the furnace support area, while storage groups C, E, F and G are stored on top of one of the Pass-through Carts. Ensure your chemical container or material is properly labeled. If there is no available room, it must be stored by in the bulk storage area. You will then need to obtain it from receiving area personnel each time you want to use it and return it to them when you are finished using it (or each time you leave the lab). Note that there is no storage of chemicals/materials in the processing lab or at any wet bench.

Chemicals will be stored in the Hong lab during spring 2021 for the E241 course. After the completion of the course, chemicals will be stored in SNF.

- Disposal: How will you dispose of any waste or excess chemical or material? In your discussions with experts and vendors, try to determine the best way to dispose of your spent chemicals and by-products. Please refer to the SNF Lab members Safety Manual for the different methods of waste disposal that are available in the lab.

Excess chemical during spin coating will be disposed in the Ziploc bags provided by SNF and in the sealed garbage container next to the Headway. Because NIPAM is hazardous, excess beyond that associated with spin coating will be labeled and disposed in the hazardous waste bin near the lithosolv bench.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: