Request Title:  Process Ga2O3 wafers in LPCVD, PECVD tools

Requestor: 	Kelly Woo					Date:  2/26/21

Non-SNF staff, please complete the following:

Badger ID: 05963993

Company name/PI: Srabanti Chowdhury

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. Beta Ga2O3 wafers

- Vendor/manufacturer info: Kyma technologies.

http://www.kymatech.com/products-services/materials/ga2o3-related-iii2o3-materials/530-gallium-oxide-substrates

Reason for request: Ga2O3 substrates have never been used in oxide CVD deposition tools in the past. Archive for future reference.

- Process Flow:

Clean substrates at Wet Bench Flexible Solvents with Acetone (~5min) and IPA(~2min) and sonication if necessary .

Do SiO2 deposition at Flexible/All cleanliness CVD tools – thermcoLTO, hdpcvd, and ccp-dep

- Amount and form. N/A

- Storage: substrates will be stored in SNF.

- Disposal: handled like Flexible cleanliness Si substrates

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: