Request Title:  	Low temperature ALD process

Requestor: 		Gilad Zeevi					Date:  10/21/2021

Non-SNF staff, please complete the following:

Badger ID:		giladz21

Company name/PI: Subhasish Mitra

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. Deposition of thin AlxOy by atomic-layer-deposited (ALD) at 50°C.

- Vendor/manufacturer info: All materials are approved SNF cleanroom materials.

- Reason for request: We search for high quality thin gate dielectric interfacial layer to enable highly-scaled carbon nanotube field-effect transistors. Deposition of good quality thin gate-dielectric layers (~3 nm) are challenging when they are deposited on defect-free sp2 bonded carbon surfaces due to poor nucleation. See attached files for further process methods and results.

- Process Flow: The novelty (regard to processes in the SNF clean room) is the initial thin (<1nm) AlxOy deposition before turning to conventional high-k layer deposition, without breaking vacuum in the ALD chamber. We intend to apply the initial AlxOy deposition by controlling the purge time between TMA and H2O precursor pulses at stage-temperatures as low as 50 °C. The purge times should be 500ms-4000ms. The ALD cycles consisted of a ~600 ms TMA pulse, a Ar purge, a ~50 ms H2O pulse a Ar purge. See attached papers for reference process flow and application to low-dimensional transistors.

After discussion with SNF Staff Michelle Rincon, we believe the MVD tool is the best equipment to use to avoid any potential issues encountered during the process development (such as particles, clogging a manifold from excess CVD, or strain on the pump) affecting other users.

Following the AlXOY interfacial oxide deposition in MVD, a conventional HfO2 high-k dielectric will be deposited by ALD at 200°C in the Savannah, or Fiji 3.

- Amount and form. We intend to use current SNF approved chemicals and materials.

- Storage: We intend to use current SNF approved chemicals and materials.

- Disposal: We intend to use current SNF approved chemicals and materials.

References:

Iljo Kwak et al. - Low interface trap density in scaled bilayer gate oxides on 2D materials via

nanofog low temperature atomic layer deposition, Applied Surface Science 463 (2019)

G. Pitner et al. – Sub-0.5 nm Interfacial Dielectric Enables Superior Electrostatics: 65 mV/dec Top-Gated Carbon Nanotube FETs at 15 nm Gate Length, IEDM (2020).

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: