Request Title:   Nanoporous glass etching

Requestor: 	Hnin Yin Yin Nyein				Date:  10/14/2021

Non-SNF staff, please complete the following:

Badger ID: hnyein@stanford.edu

Company name/PI:  Prof. Tom Soh

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. Please provide all common names, trade names, and CAS numbers where appropriate. Include an MSDS, if available; or provide the reason, if not. Make sure to include information for any new secondary chemicals (such as a developer for a new resist). Read the MSDSs as well as the Stanford Chemical Storage Groups to determine the Storage Group Identifier and Main Hazard Class of your chemical/material.

| Chemical name | CAS | Vendor | URL |
| --- | --- | --- | --- |
| Hexafluorosilicic acid, Fluorosilicic acid, Hydrogen hexafluorosilicate | 16961-83-4 | Sigma-Aldrich | https://www.sigmaaldrich.com/US/en/product/sial/01302?context=product |
| Potassium fluoride dihydrate | 13455-21-5 | Alfa Aesar | https://www.alfa.com/en/catalog/011555/ |
| Boric acid | 10043-35-3 | Sigma-Aldrich | https://www.sigmaaldrich.com/US/en/product/sigma/b6768?context=product |
| Silica gel | 112926-00-8 | Sigma-Aldrich | https://www.sigmaaldrich.com/US/en/product/sial/236772?context=product |

- Vendor/manufacturer info: address and phone number, website URL.

See above.

- Reason for request: Please give serious thought to this. If you have any process information (application notes from the vendor, protocol from another lab, experimental methods section of an article), please include it, preferably as attachments. Ask yourself these questions: Is this the latest procedure? Are there newer/safer alternatives that will also work for my project? Will any of the current SNF approved chemicals and materials work for me?

Our goal is to make nanoporous glass (NPG) with high transmittance. The pores size should be tunable and reproducible. The attached literature has shown a process which can provide promising NPG as we desired. Although HF can etch glass, it is an isotropic etch. Therefore, it is not suitable for making nanopores.

- Process Flow: Please provide a detailed process flow description on how and where you proposed to use this chemical. This should include all Lab equipment to be used for processing your wafers once your new chemical or material has been used (even if your new material is a film that is removed, it may still pose potential contamination concerns.) Make sure to include wet benches. Please note that f the chemical/material is to be used in any the "clean" equipment, purity specifications will be needed. This is most important for chemicals/material that are not normally used for VLSI device fabrication. To be allowed into a "clean" tool, the material should MOS grade or better.

Starting material: 1x1” unprocessed microscope coverslip, taken out directly from the original box.

Container/beaker, tweezer: Plastic/Teflon

  - Cleaning glass slide with 2% HF.

    - Obtain 3 plastic beakers. One for HF and two for water.

    - Label the in-use hazardous materials for each beaker.

    - Obtain 2% HF bottle from the passthrough on the plastic cart.

    - Pour 2% HF to 400 mL mark. And put the HF label next to it.

    - Return 2% HF to the passthrough on the plastic cart.

    - Add 500 mL DI water into the other two beakers. Put labels next to each beaker.

    - Put the glass slide on a Teflon chip holder.

    - Immerse the chip holder into HF for 2 mins.

    - Raise the chip holder about HF level. Slightly shake the chip holder and transfer it into the water beaker next to it. Slightly shake it in the water.

    - Raise the chip holder about water level. Slightly shake the chip holder and transfer it into the water beaker next to it. Slightly shake it in the water.

    - Remove the holder and rinse one more time with DI water in the sink.

    - Put the holder onto a cleanroom wipe and dry the chip with N2 gun while the glass slide is still in the holder.

    - Remove the glass slide with tweezer and put it into a petri dish.

    - Pour water in the beakers into HF drain. Rinse the two water beakers with water 3 times and pour the rinsed water into HF drain.

    - Pour 2% HF into the HF drain. Rinse with water for 3 times and pour the rinsed water into HF drain.

    - Remove the labels.

  - Etching glass slide to make NPG.

    - Obtain 3 plastic beakers. One for chemical mixture (composition quantified below) and two for water.

    - Label the in-use hazardous materials for each beaker in full-name.

    - Obtain hexafluorosilicic acid bottle from the passthrough on the plastic cart. Obtain pre-made mixture of potassium fluoride dihydrate, boric acid, silica gel from the pass-through on the plastic cart.

    - Pour ~ 330 mL of the mixture. And put the label next to it.

    - Pour hexafluorosilicic acid to 400 mL mark.

    - Return them to the passthrough on the plastic cart.

    - Add 500 mL DI water into the other two beakers. Put labels next to each beaker.

    - Put the glass slide on a Teflon chip holder.

    - Immerse the chip holder into the mixture for 30-60 mins.

    - Raise the chip holder above liquid level. Slightly shake the chip holder and transfer it into the water beaker next to it. Slightly shake it in the water.

    - Raise the chip holder about water level. Slightly shake the chip holder and transfer it into the water beaker next to it. Slightly shake it in the water.

    - Remove the holder and rinse one more time with DI water in the sink.

    - Put the holder onto a cleanroom wipe and dry the chip with N2 gun while the glass slide is still in the holder.

    - Remove the glass slide with tweezer and put it into a petri dish.

    - Pour water in the beakers into properly labelled waste container. Rinse the two water beakers with water 3 times and pour the rinsed water into the waste container.

    - Pour mixture into the waste container. Rinse with water for 3 times and pour the rinsed water into the waste container.

    - Remove the in-use hazardous material labels.

    - Place back the waste container at the pass-through using the plastic cart.

    - Leave to dry the used labwares on the cleanroom wipes.

    - Spray with water to cleanup the bench and blow dry with N2 gun.

- Amount and form. How much will you bring in? Is it solid, powder or liquid? (Note: as a general rule, powders are not permitted in the cleanroom.) Do you need to mix it to use it?

| Chemical name | Amount | Form | Comments |
| --- | --- | --- | --- |
| Hexafluorosilicic acid, Fluorosilicic acid, Hydrogen hexafluorosilicate | 1 L | liquid |  |
| Potassium fluoride dihydrate | 500 mL | liquid | It will be readily mixed to desired concentration in DI water such that there is no powder brought into cleanroom. |
| Boric acid |  |  |  |
| Silica gel |  |  |  |

The above chemicals will be mixed such that final composition is 18 wt % hexafluorosilicic acid – SiO2, 3 M potassium fluoride, 4 wt% boric acid.

- Storage: Will you be storing your chemical/material at SNF? If so, please note any potential reactivity’s (this should be on the MSDS). Storage groups A, B, D and L are stored in the yellow solvent cabinet in the furnace support area, while storage groups C, E, F and G are stored on top of one of the Pass-through Carts. Ensure your chemical container or material is properly labeled. If there is no available room, it must be stored by in the bulk storage area. You will then need to obtain it from receiving area personnel each time you want to use it and return it to them when you are finished using it (or each time you leave the lab). Note that there is no storage of chemicals/materials in the processing lab or at any wet bench.

Chemicals will be stored in the chemicals pass-through.

- Disposal: How will you dispose of any waste or excess chemical or material? In your discussions with experts and vendors, try to determine the best way to dispose of your spent chemicals and by-products. Please refer to the SNF Lab members Safety Manual for the different methods of waste disposal that are available in the lab.

Chemicals will be disposed into HF drain or labelled waste container (depending on what is allowed).

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: