Request Title: Preparing liquid crystal cell with nanosphere spacers in SNF flexible clean room

Requestor: Anqi Ji					Date: Jul. 13rd, 2021

Non-SNF staff, please complete the following:

Badger ID: anqi@stanford.edu

Company name/PI: Stanford University/Prof. Mark L. Brongersma

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. 1um size silica monodisperse nanospheres in standard solvent solution.

- Vendor/manufacturer info: Sigma Aldrich

- Reason for request: To create a liquid crystal cell with uniform gap thickness, the monodisperse silica spheres are used as spacers. This technique is widely used in display industry.

- Process Flow:

- Treat one glass slide (G1) with ozone plasma for 10 min.

- Drop nanosphere spacers on a second glass slide (G2).

- Put the two glass slides (G1 and G2) together with the nanospheres in between. Rotate and press the glass slide to spread out the nanospheres uniformly. Dry both slides using nitrogen gun.

- Place glue on 4 corners of G2. Then place and press G1 onto G2 so they can bond together to form a cell. Wait for the glue to dry.

- Amount and form. 2 gram, solid spheres suspended in solvent.

- Storage: No.

- Disposal: Standard solvent waste

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: