Request Title:  Grinding, polishing, annealing, wet chemistry clean of Barium Titanate Crystals

Requestor: Chris Anderson, Daniil Lukin					Date:  11/30/21

Non-SNF staff, please complete the following:

Badger ID:	cpa, dlukin

Company name/PI: Jelena Vuckovic

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. Please provide all common names, trade names, and CAS numbers where appropriate. Include an MSDS, if available; or provide the reason, if not. Make sure to include information for any new secondary chemicals (such as a developer for a new resist). Read the MSDSs as well as the Stanford Chemical Storage Groups to determine the Storage Group Identifier and Main Hazard Class of your chemical/material.

Names: BTO, BaTiO3, Barium Titanate

CAS: 12047-27-7

MSDS attached

This is a solid chip/crystal. Not a powder.

Barium poisoning if ingested

- Vendor/manufacturer info: address and phone number, website URL.

MTI Corporation

860 S. 19th Street, Richmond, CA 94804-3809

Phone: 510-525-3070

Email: sales@mtixtl.com (Crystal Dept.)

https://www.mtixtl.com/

- Reason for request: Please give serious thought to this. If you have any process information (application notes from the vendor, protocol from another lab, experimental methods section of an article), please include it, preferably as attachments. Ask yourself these questions: Is this the latest procedure? Are there newer/safer alternatives that will also work for my project? Will any of the current SNF approved chemicals and materials work for me?

BaTiO3 is an excellent electro-optical and nonlinear optics material. Building on our expertise with SiC fabrication of thin films, our lab would like to create thin films of this material bonded to SOI or Si wafers. This material is required because it is the material we would like to study due to its unique properties.

Process Flow: Please provide a detailed process flow description on how and where you proposed to use this chemical. This should include all Lab equipment to be used for processing your wafers once your new chemical or material has been used (even if your new material is a film that is removed, it may still pose potential contamination concerns.) Make sure to include wet benches. Please note that f the chemical/material is to be used in any the "clean" equipment, purity specifications will be needed. This is most important for chemicals/material that are not normally used for VLSI device fabrication. To be allowed into a "clean" tool, the material should MOS grade or better.

SNF

1. Sample Dicing (DISCO)

- standard hub blade

2. Clean sample (Flexcorr, flexsolv wet benches)

- Acetone, IPA, Piranha, HF

3. [sample bonding is done manually in our lab, no equipment required]

4. Anneal in Thermco 4 at temperature 500-800C.

5. BaTiO3 thinning (DISCO backgrinder)

- We will use specialized grinding wheels that belong to the Vuckovic group (dlukin is superuser on the tool and is qualified to replace grinding wheels). We have ground a number of different materials and are confident that small chips of this medium-hardness material will not cause issues for the instrument -- even if grinding does not work as planned, the only negative impact, if at all, could be on the grinding wheel, which does not affect other users because it belongs to our group.

6. CMP polishing of BaTiO3 (GnP POLI-400L)

- Standard silica slurry will be tried first, in full compatibility with the gold-contaminated metal platen and head. We may then consider trying a different slurry and polishing pad (using the Vuckovic platen), but that would be a separate PROM request.

SNSF (outside SNF)

7. HSQ hard mask/ebeam patterning

8. Ion Milling

9. HF undercut

SNF

10. Possible extra  Si undercut step (XACTIX)

- standard gold contaminated mode

- Amount and form. How much will you bring in? Is it solid, powder or liquid? (Note: as a general rule, powders are not permitted in the cleanroom.) Do you need to mix it to use it?

Solid chips. About 5x5 mm, a few of pieces

- Storage: Will you be storing your chemical/material at SNF? If so, please note any potential reactivity’s (this should be on the MSDS). Storage groups A, B, D and L are stored in the yellow solvent cabinet in the furnace support area, while storage groups C, E, F and G are stored on top of one of the Pass-through Carts. Ensure your chemical container or material is properly labeled. If there is no available room, it must be stored by in the bulk storage area. You will then need to obtain it from receiving area personnel each time you want to use it and return it to them when you are finished using it (or each time you leave the lab). Note that there is no storage of chemicals/materials in the processing lab or at any wet bench.

Not stored in SNF

- Disposal: How will you dispose of any waste or excess chemical or material? In your discussions with experts and vendors, try to determine the best way to dispose of your spent chemicals and by-products. Please refer to the SNF Lab members Safety Manual for the different methods of waste disposal that are available in the lab.

Solid waste bag. If large chunks or cleaved pieces, sharps container.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: