Request Title:  InP Quantum Dots in mixed solvents, ver 3

Requestor: David Viveros Salazar					Date:  03/20/2019

Non-SNF staff, please complete the following:

Badger ID: david@resonancelabs.io

Company name/PI: Resonance Labs, Inc./David Viveros Salazar

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. Please provide all common names, trade names, and CAS numbers where appropriate. Include an MSDS, if available; or provide the reason, if not. Make sure to include information for any new secondary chemicals (such as a developer for a new resist). Read the MSDSs as well as the Stanford Chemical Storage Groups and the Stanford Chemical Safety Data Base sections on this website to determine the Storage Group Identifier and Main Hazard Class of your chemical/material.

Common Names:

InP quantum dots (QD) in mixed solvents

  - 45+/-10% Proylene glycol monomethyl ether acetate (PGMEA): CAS-No 108-65-6

  - 30 +/- 10% Proprietary photoactive resin

  - 19 +/- 10% reaction products with indium zinc phosphide selenide sulfide: CAS-No 1776097-03-0

  - 6 +/- 5% Titanium dioxide: CAS-No 13463-67-7

Please see attached SDS.

- Vendor/manufacturer info: address and phone number, website URL.

Nanosys Inc.

233 South Hillview Drive

Milpitas, CA 95035

United States

Phone: 408-240-6700

Website URL: nanosysinc.com

- Reason for request: Please give serious thought to this. If you have any process information (application notes from the vendor, protocol from another lab, experimental methods section of an article), please include it, preferably as attachments. Ask yourself these questions: Is this the latest procedure? Are there newer/safer alternatives that will also work for my project? Will any of the current SNF approved chemicals and materials work for me?

This is a new process for our company. We are using a commercially available photoresist that is being used in a new and unique way. We are unaware of materials currently available in the lab that behave, optically, in the same manner as this material that we are submitting for review. When photoexcited, this material emits red and green light. This is the primary requirement for our application.

- Process Flow: Please provide a detailed process flow description on how and where you proposed to use this chemical. This should include all Lab equipment to be used for processing your wafers once your new chemical or material has been used (even if your new material is a film that is removed, it may still pose potential contamination concerns.) Make sure to include wet benches. Please note that f the chemical/material is to be used in any the "clean" equipment, purity specifications will be needed. This is most important for chemicals/material that are not normally used for VLSI device fabrication. To be allowed into a "clean" tool, the material should MOS grade or better.

Substrate: 4” fused silica or quartz wafers

  - Prepare Wafers

    - Use HMDS yes oven for HMDS treatment of wafers

  - Spin Coat and Pre-bake

    - Transport HMDS coated wafers in cassette to laurell-G in the ExFab

    - Cover workspace with aluminum foil

    - Cover hot plate with aluminum foil

    - Cover inside of Laurell containment volume with aluminum foil

    - Prepare Ziploc bags for transfer of waste

    - Transfer wafer from cassette onto Laurell chuck

    - Place cover on Laurell

    - Retrieve InP from storage container (the storage container will either be in the ExFab or in a separate travel container provided by Resonance Labs)

    - Fill out blue slip for InP

    - Verify all PPE has been put on including face shield

    - Set speed and timer on Laurell

    - Use syringe to drop material onto spinning wafer

    - Place contaminated syringe into Ziploc bag and place in waste container

    - Transfer wafer onto hotplate

    - Pre-bake wafer at 100 C for 2 min

    - Remove aluminum foil from inside of Laurell containment volume and place contaminated foil into Ziploc bag and place in waste container

    - Wipe the inside of the Laurell with acetone and place waste in a Ziploc bag and place in waste container

    - Transfer pre-baked wafer into cassette

  - Expose

    - Transport wafer to litho room

    - Use karlsuss for UV exposure

  - Develop

    - Transport wafers back to the laurell-G in the ExFab

    - Use the wet bench next to laurell-G to develop wafers (Resonance Labs will use their own glassware for development of wafers)

    - Fill large beaker with developer

    - Place wafer in the large beaker

    - Blow dry wafer

  - Post-bake

    - Place new aluminum foil on hot plate

    - Place wafer on hot place

    - Post-bake at 180 C for 60 min

  - Imaging

    - Use scope3 to image the patterned photoresist.

- Amount and form. How much will you bring in? Is it solid, powder or liquid? (Note: as a general rule, powders are not permitted in the cleanroom.) Do you need to mix it to use it?

Small containers with sealable caps will be used to contain the liquid material. Two amounts will be brought into lab. Initially an amount of 20g will be contained in the bottles.

- Storage: Will you be storing your chemical/material at SNF? If so, please note any potential reactivity’s (this should be on the MSDS). Storage groups A, B, D and L are stored in the yellow solvent cabinet in the furnace support area, while storage groups C, E, F and G are stored on top of one of the Pass-through Carts. Ensure your chemical container or material is properly labeled. If there is no available room, it must be stored by in the bulk storage area. You will then need to obtain it from receiving area personnel each time you want to use it and return it to them when you are finished using it (or each time you leave the lab). Note that there is no storage of chemicals/materials in the processing lab or at any wet bench.

The material is in liquid form and it will need to be refrigerated. If I can store the material in the lab refrigerator at 5 C, then I would like to keep it in the lab. Otherwise I will transport it myself when I come into lab. According to the SNF Storage Group Guide, this material is in Group L.

- Disposal: How will you dispose of any waste or excess chemical or material? In your discussions with experts and vendors, try to determine the best way to dispose of your spent chemicals and by-products. Please refer to the SNF Lab members Safety Manual for the different methods of waste disposal that are available in the lab.

Spin coated residue will be disposed of in plastic bags and placed in the chemical waste containers. During development, the developer and exposed photoresist will be disposed of in the wet bench next to laurell-G.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: