Request Title: Sugar Layer Processing

Requestor: Arash Afsarifard						Date:  11/26/2019

Non-SNF staff, please complete the following:

Badger ID: asafsari

Company name/PI: Genapsys Inc.

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material

The solution I am using has a still varying amount of 3 ingredients:

Deionized Water-Already present in lab so MSDS should not be necessary

Trehalose or mycose or tremalose

MSDS of Trehalose: https://www.sigmaaldrich.com/MSDS/MSDS/DisplayMSDSPage.do?country=US&language=en&productNumber=T9449&brand=SIGMA&PageToGoToURL=https%3A%2F%2Fwww.sigmaaldrich.com%2Fcatalog%2Fproduct%2Fsigma%2Ft9449%3Flang%3Den

Sucrose

MSDS of Sucrose: https://www.sigmaaldrich.com/MSDS/MSDS/DisplayMSDSPage.do?country=US&language=en&productNumber=S8501&brand=SIGMA&PageToGoToURL=https%3A%2F%2Fwww.sigmaaldrich.com%2Fcatalog%2Fproduct%2Fsigma%2Fs8501%3Flang%3Den

- Vendor/manufacturer info:

Sigma-Aldrich

3050 Spruce Street, St. Louis, MO 63103

1 (800) 325-3010

https://www.sigmaaldrich.com/united-states.html

- Reason for request:

I need a way to determine the thickness of the material when layered on a wafer with our concentrations of the solution and layering changing.

- Process Flow:

I would need to plasma clean the wafer before putting on the sugar layer. So I would use the MRC to condition the SiO2 wafer. Next, I would like to use the Headway to manually spin and bake the sugar on a hotplate as a layer onto the wafer. If this is not possible, I will take the wafer out, spin and heat bake it on at my own lab, then bring it back for the next steps. At this point, the sugar is a glass, solid layer on top that does not dissolve out particles. It is somewhat sticky, similar to photoresist. I would then use a tool to determine the sugar layer’s thickness. I am considering the Filmetrics, Ellipsometer and Profilometer. It would be best to do the 1st or 2nd option as those are purely optical based.

- Amount and form.

The sugar is in an aqueous solution. The sugar is completely dissolved and does not reform in solution. I would mix it at my own lab and thus I would not need to bring the powders of sugars into the lab, only the fully dissolved solution. I would bring in 20-50 mL at a time.

- Storage:

The chemical is not intrinsically Reactive, Flammable or Combustible. It would be stored in Chemical Group G. I can also just bring one time use solutions every time if storage in SNF of this chemical is cause for concern.

- Disposal:

I would like to be able to dispose of this chemical in general waste as none of the materials are hazardous. If use of the Headway is permitted, then I would dispose of the sugar there as it is spin coated on. If coating is necessary to be done outside SNF, then there will be no need for disposal of the substance as I would not need to bring in the solution.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: