Process or Materials Review Request Form

Request Title: Request to use Aqua Regia to wet etch Pt

Requestor: Archana Kumar                                                        Date:  05/08/2019

Non-SNF staff, please complete the following:

Badger ID:  archana_kumar@amat.com

Company name/PI: Applied Materials

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material.

This request is for a non-standard process with standard available chemicals in SNF. Aqua Regia is a mixture of concentrated nitric acid and concentrated hydrochloric acid in a 1:3 molar ratio (1:4 volume ratio for 37% HCl and 69% HNO3). Both Nitric acid and hydrochloric acid are standard available approved chemicals in SNF and will be mixed in a beaker at the time of use. SNF versions of MSDS apply (links on SNF wiki).

https://fscimage.fishersci.com/msds/16550.htm

https://fscimage.fishersci.com/msds/11155.htm

- Vendor/manufacturer info

Standard SNF provided chemicals.

- Reason for request

This mixture will be used to test the selective etch of Pt metal on Pt silicide. Thin <50nm layers of Pt will be etched from 1”x1” Silicon pieces. This specific process is necessary for comparison with a customer flow in a commercial fabrication facility and cannot be substituted with another process due to the nature of customer deliverables for this project.

- Process Flow:

Both nitric acid and hydrochloric acid are standard available approved chemicals in SNF and will be mixed in a beaker at wbflexcorr-1/2 at the time of use.

- Starting substrate: Oxide patterned silicon pieces (1.2”x1.2”)

- 50nm Pt deposited at Lesker sputter at 200W

- Anneal in N2, 550C 5 min AW610_R to form PtSi

- Anneal in O2, 550C, 2 min, AW610_R

- Etch unreacted Pt from coupon using Aqua Regia dip. Nitric acid will be added to the hydrochloric acid in that order, as per recommended procedure. Rinse in DI water, N2 dry.

Full PPE will be used. If needed I will reserve both sides of the bench for other users’ safety. The process will be done during daytime office hours with staff members around if needed.

Web references with the chemical equations etc:

https://en.wikipedia.org/wiki/Aqua_regia

https://www.thoughtco.com/making-aqua-regia-acid-solution-603641

- Amount and form:

No new chemical will be brought in. Both nitric acid and hydrochloric acid are standard available approved chemicals in SNF and will be mixed in a beaker at the time of use. Estimated volume of use -  200ml perhaps once a week for 2 or 3 weeks.

- Storage:

No mixture will be stored. The mixture will be made and used within 1 hour at wbflexcorr-1/2 for the etch process.

- Disposal:

The used chemical will have etched metal (Pt), so it will be collected locally for disposal in an empty, clean, decontaminated chemical container (compatible with nitric and hydrochloric acids), labeled as hazardous waste with a tag noting its contents and placed in the chemical passthrough for disposal.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date:

V1.0