Request Title:  	Aqua Regia for Surface Clean

Requestor: 			Carol Huang				Date:  11/13/19

Non-SNF staff, please complete the following:

Badger ID:			chuang@ganworks.com

Company name/PI:                  GaNWorks

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. 
Aqua Regia: Mixture of 37% Hydrochloric Acid/Nitric Acid (3:1)

Please provide all common names, trade names, and CAS numbers where appropriate. Include an MSDS, if available; or provide the reason, if not. Make sure to include information for any new secondary chemicals (such as a developer for a new resist). Read the MSDSs as well as the Stanford Chemical Storage Groups to determine the Storage Group Identifier and Main Hazard Class of your chemical/material.

- Vendor/manufacturer info: address and phone number, website URL.

Hydrochloric Acid 37% and Nitric Acid, both in stock at SNF

- Reason for request: Please give serious thought to this. If you have any process information (application notes from the vendor, protocol from another lab, experimental methods section of an article), please include it, preferably as attachments. Ask yourself these questions: Is this the latest procedure? Are there newer/safer alternatives that will also work for my project? Will any of the current SNF approved chemicals and materials work for me?

Aqua regia is a well known surface treatment for GaN post MOCVD growth to remove surface oxide and help achieve low and consistent contact resistance.

- Process Flow: Please provide a detailed process flow description on how and where you proposed to use this chemical. This should include all Lab equipment to be used for processing your wafers once your new chemical or material has been used (even if your new material is a film that is removed, it may still pose potential contamination concerns.) Make sure to include wet benches. Please note that f the chemical/material is to be used in any the "clean" equipment, purity specifications will be needed. This is most important for chemicals/material that are not normally used for VLSI device fabrication. To be allowed into a "clean" tool, the material should MOS grade or better.

- RTA Anneal  Aqua Regia surface clean in beaker at wbflexcorr  BOE at wbflexcorr  Metal Evaporation

- RTA Anneal  Aqua Regia surface clean in beaker at wbflexcorr  Yes Oven  headway  Karl Suss  develop bench  BOE at wbflexcorr  Metal Evaporation  liftoff at wbflexsolv

- Amount and form. How much will you bring in? Is it solid, powder or liquid? (Note: as a general rule, powders are not permitted in the cleanroom.) Do you need to mix it to use it?

We will mix hydrochloric acid 37% with nitric acid (3:1) in a 500ml beaker

- Storage: Will you be storing your chemical/material at SNF? If so, please note any potential reactivity’s (this should be on the MSDS). Storage groups A, B, D and L are stored in the yellow solvent cabinet in the furnace support area, while storage groups C, E, F and G are stored on top of one of the Pass-through Carts. Ensure your chemical container or material is properly labeled. If there is no available room, it must be stored by in the bulk storage area. You will then need to obtain it from receiving area personnel each time you want to use it and return it to them when you are finished using it (or each time you leave the lab). Note that there is no storage of chemicals/materials in the processing lab or at any wet bench.

Aqua Regia mixture will not be stored

- Disposal: How will you dispose of any waste or excess chemical or material? In your discussions with experts and vendors, try to determine the best way to dispose of your spent chemicals and by-products. Please refer to the SNF Lab members Safety Manual for the different methods of waste disposal that are available in the lab. 

Aqua Regia waste will be disposed using aspirator in the wbflexcorr bench once the chemical reaction is done and chemical is cooled

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: