Process or Materials Review Request Form

Request Title:           MICROPOSIT™ LOL™ 1000 LIFT OFF LAYER

Requestor:         Robert Xu                                                Date:   5/29/19

Non-SNF staff, please complete the following:

Badger ID:              rxu@raxium.com

Company name/PI: Raxium,Inc/ Tai Nguyen

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material.

MICROPOSIT™ LOL™ 1000 LIFT OFF LAYER. SDS attached. It will be stored in the same cabinet as LOL 2000 in litho room

- Vendor/manufacturer info:

Vendor: Microchem address 200 Flanders Road Westborough, MA 01581

Manufacturer: Dow chemical

phone (617) 965-5511 Ext. 1

www.microchem.com

- Reason for request:

SNF has thicker version of the liftoff coating: LOL2000. It is good for >2um patterns.  For 2um pattern, LOL1000 is needed. LOL1000 will be used as same way as LOL2000 on Headway manual coated.

- Process Flow:

  - SNF standard HMDS YesOven bake

  - LOL manual coating on Headway at 3000 RPM

  - WhiteOven bake at 190C/30min

  - SVG coat track2 0.9um 955 resist coat without vapor prime.

  - SRD clean

  - ASML mask patterning

  - SVG Develop PEB (Program 9/3)

  - SVG Develop (Program 2/1)

  - Raxium fab metal deposition and liftoff.

- Amount and form: One quart liquid bottle, no mixing.

- Storage: LOL1000 will be stored in yellow solvent cabinet in Litho bay.

- Disposal: Unused LOL1000 will be returned to Raxium, Inc.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date:

V1.0