Request Title:  InSb Sputter Target for Lesker Sputter

Requestor: Pascal Stasner						Date:  02/20/19

Non-SNF staff, please complete the following:

Badger ID: stasner

Company name/PI: Fritz Prinz

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material.

Name: Indium antimonide, InSb or Indium monoantimonide.

CAS number: 1312-41-0

MSDS provided in attachment.

Storage: store in a cool dry place in a tightly sealed container. Stable under recommended storage conditions, Store apart from / reacts with oxidizing agents. No incompatible conditions. Hazardous decomposition products: Metal oxide fume.

Storage Group: G

Hazard class: Toxic substances

- Vendor/manufacturer info:

Address:

MSE Supplies LLC

4400 E Broadway Blvd, Suite 600

Tucson, AZ 85711, USA

Phone number: (520)-789-6673

Website: https://www.msesupplies.com/pages/sputtering-targets

- Reason for request:

Process information: In previous experiments a 2-inch InSb sputtering target was used in a sputter without a heating stage. The goal is an InSb thin film (around 100 nm) that is as crystalline and as dense as possible. The lowest possible Argon pressure was used while still maintaining ignition of plasma (0.27 Pa). The RF plasma power was set at 100 W. The deposition time was around 10 min for 100 nm. However, the result of sputtered InSb at room temperature was an amorphous thin film. Post annealing was used to crystallize the thin film. This led to an agglomeration of pores and inevitably to large holes in the thin film. SEM pictures of the problematic hole formation after post-annealing have been attached.

Deposition during elevated temperatures (up to 450 °C) will presumably lead to a crystallized film that has no/less pores which will lead to a decrease in holes in the thin film. Since our sputter does not have a heating stage, we want to use the InSb target in the Lesker sputter in SNF.

The project is dependent on the use of InSb as III/V-semiconductor and therefore other materials currently available for the Lesker sputter cannot be used as alternative.

- Process Flow:

The InSb target will be used in a sputter system. Afterwards, the sheet resistance of the InSb thin film will be measured with a four-probe-measurement system at SNF. The purity of the InSb is 99.999%

- Amount and form.

It is a solid sputter target. Diameter: 2 inch. Thickness: 0.125 inch. Bonded to a 2mm thick Cu backing plate

- Storage:

Target will not be stored at SNF.

- Disposal: There will not be waste material as it is a sputtering target.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: