Request Title:  	Request for Dupont EKC 265

Requestor: 	Kee-Hyun Paik						Date:  2019/10/03

Non-SNF staff, please complete the following:

Badger ID: paik@multerra.bio

Company name/PI: Multerra Bio, Inc./Kee-Hyun Paik

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material.

Dupont Plasmasolv EKC 265 (2-(2-Aminoethoxy)ethanol (55-65%), Hydroxylamine (17.5%), Pyrocatechol (4.97%))

Storage group is L (flammables, combustables and organic solvents)

- Vendor/manufacturer info: Vendor: Maroon Group

537 Raymond Blvd, Newark, NJ 07105

(973) 465 1122 x 1111

Web URL www.maroongroupllc.com

- Reason for request:

Removal of post etch residue from performing Ti etching in PT-MTL that has been difficult to remove using heated ashing.

- Process Flow:

- Reserve both wbflexcorr 3 and 4. Activate wbflexcorr 3. (While working with EKC265, other people can not work aside)

- Obtain and label a waste container.

- Fill blue “in-use hazardous chemical” tags

- Fill a beaker with EKC265, and place a thermometer into the beaker.

- Slowly heat up this beaker on the hotplate to 65 ~75 degree C. (Monitor the temperature with the thermometer, and stir the liquid frequently.)

- Load the wafers into a cassette.

- Dip the cassette into the heated EKC265 solution. Let the samples soak in EKC265 for 30min.

- Prepare three beakers of DI water

- Dip the cassette up and down inside the first DI water 5 times

- Repeat last step with the other 2 DI beakers.

- Place the last DI beaker under running DI water, and let it overflow for 5 min.

- Dry the samples with N2 gun.

- Collect EKC265 waste with the waste bottle. Fully rinse all beakers, thermometer, and the cassette, Collect the rinsed DI water with the waste bottle if it is colored.

- Place the waste bottle in room 162A

- Amount and form. I will bring in a standard 1Gal container sold by the manufacturer in liquid form. The product is to be used without mixing.

- Storage: Storage group L, I will use the yellow solvent cabinet if there is room. Otherwise storage will be arranged in bulk storage area.

- Disposal: Defer to SNF staff. Used chemical can be collected for separate disposal or if appropriate added to the solvent waste stream.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: