Request Title:  	Request for Dupont EKC 265

Requestor: 	Kee-Hyun Paik						Date:  2019/10/03

Non-SNF staff, please complete the following:

Badger ID: paik@multerra.bio

Company name/PI: Multerra Bio, Inc./Kee-Hyun Paik

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material.

Dupont Plasmasolv EKC 265 (2-(2-Aminoethoxy)ethanol (55-65%), Hydroxylamine (17.5%), Pyrocatechol (4.97%))

Storage group is L (flammables, combustables and organic solvents)

- Vendor/manufacturer info: Vendor: Maroon Group

537 Raymond Blvd, Newark, NJ 07105

(973) 465 1122 x 1111

Web URL www.maroongroupllc.com

- Reason for request:

Removal of post etch residue from performing Ti etching in PT-MTL that has been difficult to remove using heated ashing.

- Process Flow:

- Use the metal solvent cart to bring EKC265 in its container to WB-SOLVENT

- Transfer needed amount of EKC265 to crystallization dish of appropriate size

- Using either the sonicator(CTB) or hot plate, heat EKC265 to 65oC with wafers/chips in the crystallization dish.

- Allow chips to be cleaned in EKC265 for 20min.

- Remove crystallization dish from heat source and allow to cool down.

- Remove chips from EKC265 into another crystallization dish with Isopropanol.

- Wash chips/wafers in IPA for 10 min.

- Dry chips by airgun

- Amount and form. I will bring in a standard 1Gal container sold by the manufacturer in liquid form. The product is to be used without mixing.

- Storage: Storage group L, I will use the yellow solvent cabinet if there is room. Otherwise storage will be arranged in bulk storage area.

- Disposal: Defer to SNF staff. Used chemical can be collected for separate disposal or if appropriate added to the solvent waste stream.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: