Request Title:

Requestor: Yimeng Sun							Date:  04/08/2019

Non-SNF staff, please complete the following:

Badger ID:	mengsnf0220@gmail.com

Company name/PI: Raxium/Tai Nguyen

Send completed form to: snf-promcommittee@lists.stanford.edu

| Chemical Names | Component | CAS Number |
| --- | --- | --- |
| EKC640 Semi-Aqueous Post-Etch Residue Removal | N,N-Dimethyacetamide | 127-19-5 |
|  | Ammonium Fluoride | 12125-01-8 |
|  | 2,2’-Iminodiethanol | 111-42-2 |

The storage group for this chemical is considered to be L, since it is combustible liquid, and it is not compatible with strong acid. See attached SDS.

- Vendor/manufacturer info: EKC Technology, Inc. 2520 Barrington Court Hayward, CA94545-1133, USA. Phone number: (510) 784-9105

Website: http://www.dupont.com/products-and-services/electronic-electrical-materials/semiconductorfabrication-packaging-materials/brands/ekc-photoresist-and-redidue-removers.html

- Reason for request:

We are suffering from post-dry etch photoresist residue, and EKC640 seems to be the most effective way to remove these veils. See attached application notes.

- Process Flow:

I will be using wbflexcorr3 and 4 for this process:

- Reserve and activate wbflexcorr 3.

- Obtain and label a waste container.

- Fill blue “in-use hazardous chemical” tags.

- Fill a Teflon beaker with EKC640.

- Load the sapphire wafers into a cassette.

- For room temperature processes: Dip the cassette into the EKC640 solution. Let the samples soak in EKC640 for 2min.

- For 40C application: Heat EKC640 to 40C, dip the cassette into the solution for 5min.

- Prepare three beakers of DI water.

- Dip the cassette up and down inside the first DI water 5 times

- Repeat last step with the other 2 DI beakers.

- Place the last DI beaker under running DI water, and let it overflow for 5 min.

- Dry the samples with N2 gun.

- Collect EKC640 waste with the waste bottle. Fully rinse all beakers and the cassette, Collect the rinsed DI water with the waste bottle.

- Place the waste bottle in room 162A.

- Amount and form. It is in the form of liquid. I will be bringing a one gallon container of EKC640 in.

- Storage:

Yes, I plan to store this at SNF inside the solvent cabinet. It is incompatible with strong acids. Its hazardous decomposition products is ammonia.

- Disposal: 1 Obtain a clean, empty waste container. (Do not use empty chemical containers, which have not been decontaminated.) The chemical labels on these containers should be defaced; if not, use the large black marker located there to cross out the label. The clean containers that are supplied are made of polypropylene, which is inert to most, but not all, chemicals used in the lab. 2 Obtain a blank hazardous waste disposal labels. Blank labels and clean bottle tops, are available next to the clean containers. Fill out the pertinent information on the hazardous waste disposal label. Attach the label to the waste container (they can be tied to a handle.) 4 Pour the used chemical into the labeled waste container. This should be done at the wet bench, using a chemically compatible funnel for safe pouring. Rinse the container you used for processing with water three times, pouring the rinse water each time into the waste container. Pour the water used to rinse the substrates into the waste container. 5 Cap the container, making sure that the outside of the container is clean and dry. Make sure the hazardous waste label is securely attached. 6 Transport the container using the transfer cart. Place the container in Room 162A.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: