Request Title:  Vanadium dioxide anneal and patterning

Requestor: Aditya Sood						Date: 01/24/2019

Non-SNF staff, please complete the following:

Badger ID: aditsood (Email: aditsood@stanford.edu )

Company name/PI: Aaron Lindenberg

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. Please provide all common names, trade names, and CAS numbers where appropriate. Include an MSDS, if available; or provide the reason, if not. Make sure to include information for any new secondary chemicals (such as a developer for a new resist). Read the MSDSs as well as the Stanford Chemical Storage Groups and the Stanford Chemical Safety Data Base sections on this website to determine the Storage Group Identifier and Main Hazard Class of your chemical/material.

Vanadium (IV) dioxide (VO2). MSDS attached for powdered VO2 (CAS number 12036-21-4). Our samples are NOT powders, they are ~50 nm thick continuous, polycrystalline films sputtered onto SiN/Si substrates.

Note: there is already an approved PROM request for the same material (although in single crystal form) – from: Stephanie Bohaichuk, approved by PROM committee on: 11/20/2015. This is also attached.

- Vendor/manufacturer info: address and phone number, website URL.

VO2 films will be deposited using sputtering at the lab of Prof. Shriram Ramanathan (Purdue University, West Lafayette, Indiana). Website: https://shriram-ramanathan.org/

- Reason for request: Please give serious thought to this. If you have any process information (application notes from the vendor, protocol from another lab, experimental methods section of an article), please include it, preferably as attachments. Ask yourself these questions: Is this the latest procedure? Are there newer/safer alternatives that will also work for my project? Will any of the current SNF approved chemicals and materials work for me?

VO2 is an insulator-metal phase transition material. We intend to fabricate devices that will induce the phase transition under applied voltage. While the VO2 will be deposited outside of SNF, we plan to perform the following processes at SNF: (1) anneal films under O2+Ar ambient in the ALD system (Fiji2). Conditions: pressure ~100-200 mTorr, temperature ~ 350 C, time ~30 minutes. (2) photolithography: Headway spinner, hot plates, Heidelberg, solvent wet bench.

- Process Flow: Please provide a detailed process flow description on how and where you proposed to use this chemical. This should include all Lab equipment to be used for processing your wafers once your new chemical or material has been used (even if your new material is a film that is removed, it may still pose potential contamination concerns.) Make sure to include wet benches. Please note that f the chemical/material is to be used in any the "clean" equipment, purity specifications will be needed. This is most important for chemicals/material that are not normally used for VLSI device fabrication. To be allowed into a "clean" tool, the material should MOS grade or better.

Starting substrate: SiN (50 nm)/Si with etched membranes. Substrates are 4 inch wafers. VO2 is sputtered outside SNF to a thickness of ~50 nm (considered “gold contaminated”). Following describes the subsequent process flow at SNF:

[Fiji2]: used to anneal sample at 350 C for ~30 minutes under O2+Ar flow, total pressure ~100-200 mTorr. Have discussed this process with Michelle Rincon.

[hotplate] 115 C, 1 min

[headway] spincoat LOL2000 – 5000 rpm, 60 s

[white oven] 160 C, 13 min

[headway] spincoat SPR 3612 – 4000 rpm, 30 s

[hotplate] 90 C, 1 min

[heidelberg] Standard alignment + patterning

[hotplate] 115 C, 1 min

[develop] manual develop, MF-26A 40 sec

[hotplate] 115 C, 1 min

[deposit metal using e-beam evap. outside SNF: Ti (3 nm)/Au (50 nm)]

[wbflexsolv] liftoff – Acetone, Remover PG, Isopropanol (room temperature)

- Amount and form. How much will you bring in? Is it solid, powder or liquid? (Note: as a general rule, powders are not permitted in the cleanroom.) Do you need to mix it to use it?

VO2 films are solid continuous layers deposited onto SiN/Si substrate, ~50 nm thick (not powders). Substrates are 4 inch wafers.

- Storage: Will you be storing your chemical/material at SNF? If so, please note any potential reactivity’s (this should be on the MSDS). Storage groups A, B, D and L are stored in the yellow solvent cabinet in the furnace support area, while storage groups C, E, F and G are stored on top of one of the Pass-through Carts. Ensure your chemical container or material is properly labeled. If there is no available room, it must be stored by in the bulk storage area. You will then need to obtain it from receiving area personnel each time you want to use it and return it to them when you are finished using it (or each time you leave the lab). Note that there is no storage of chemicals/materials in the processing lab or at any wet bench.

Samples will be stored in dry box outside SNF.

- Disposal: How will you dispose of any waste or excess chemical or material? In your discussions with experts and vendors, try to determine the best way to dispose of your spent chemicals and by-products. Please refer to the SNF Lab members Safety Manual for the different methods of waste disposal that are available in the lab.

- We do not expect to remove/etch away any VO2 during our process.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: