Request Title:  bring S1813 coated glass slides to cleanroom

Requestor:  Alex Xing					Date:  12/04/2019

Non-SNF staff, please complete the following:

Badger ID: alex.xing@10xgenomics.com

Company name/PI: 10x Genomics

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material.

Borosilicate glass slides coated with Micropost S1800 Series Photoresist S1813,

- Vendor/manufacturer info:

Kayaku, https://kayakuam.com/products/microposit-s1800-series-broadband-resists/

- Reason for request: we have been using this photoresist S1813 coated glass surface for biopatterning and achieves good results. We would like to bring the coated slides and fabricate micro patterns (1.5um) using the Karl Suss setup.

- Process Flow:

Step 0

Use Karl Suss setup to expose 1”x3” glass slide (1mm thick glass slide, the glass slide is

pre-coated with S1813 photoresist and soft-baked before entering SNF)

Step 1:

Develop the photoresist in MF26A developer at wet bench (wbmiscres) and check under optical microscope.

- Amount and form.

5~10 slides a time. It will be dry glass slides.

- Storage: I will not store these slides in SNF.

- Disposal: The waste generated from the developer will be disposed following the standard procedures at SNF.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: