Process or Materials Review Request

Request Title: Adhesion Promotor for Nanoscribe IP Resists

Requestor:   Linda Whittelsey                                    Date:  02/13/2019

Non-SNF staff, please complete the following:

Badger ID:   lwhittel@comcast.net

Company name/PI: Elegen Bio/ Alex Sugarbaker

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. Please provide all common names, trade names, and CAS numbers where appropriate. Include an MSDS, if available; or provide the reason, if not. Make sure to include information for any new secondary chemicals (such as a developer for a new resist). Read the MSDSs as well as the Stanford Chemical Storage Groups and the Stanford Chemical Safety Data Base sections on this website to determine the Storage Group Identifier and Main Hazard Class of your chemical/material.

3-(Trimethoxysilyl)propyl methacrylate for silanization of glass substrates for use with the Nanoscribe printer. Synonyms: Silane A174, [3-(Methacryloyloxy)propyl]trimethoxysilane. CAS: 2530-85-0.

MSDS: https://www.sigmaaldrich.com/MSDS/MSDS/DisplayMSDSPage.do?country=US&language=en&productNumber=M6514&brand=SIGMA&PageToGoToURL=https%3A%2F%2Fwww.sigmaaldrich.com%2Fcatalog%2Fproduct%2Fsigma%2Fm6514%3Flang%3Den

Storage Group L.  Plan to store in group L refrigerator in service chase.

- Vendor/manufacturer info: address and phone number, website URL.

Available from Sigma Aldrich as M6514.

Sigma-Aldrich

Customer Support

PO Box 14508

St. Louis, MO 63178

Phone:1-800-325-3010

Fax: 1-800-325-5052

www.sigmaaldrich.com

- Reason for request:   This priming process is recommended by Nanoscribe and we have done the priming off site in the recent past.  The priming definitely improves the adhesion of the IP-S resist to ITO substrate surface during the development process.  I have attached the document from Nanoscribe describing the priming process.  (Scroll down to Step 2 on page 2 of the document ResistAdhesionNotesForIPS.pdf).  We would like to be able to reduce travel and ferrying of ITO Meso substrates to and from our offsite lab space and SNF for this one process done prior to printing on the nanoscribe.

- Process flow:  This non-clean process will be done with dirty glassware (found at WBFLEXCORR3 & 4). A small graduated cylinder and small glass beaker (100 or 150 ml) will be used at either the exfab solv bench or wbsolv if space is limited at exfabsolv.  The beaker will be “sealed” with either aluminum foil or parafilm (if allowed) or plastic “cling wrap” during the substrate immersion in the priming solvent solution. These materials will be disposed as solid solvent waste in a sealed baggie with any contaminated wipes and placed in a solid solvent waste can.  The priming solvent solution will be disposed of by pouring into the solvent waste containment carboy at the bench where the processing will be done.  Dirty Au contaminated tweezers will be used to handle the substrate. Glassware and tweezers will be rinsed with acetone and isopropyl after use and allowed to air dry on the bench before transferring back to the storage cabinet across from FLEXCORR3 & 4.  Below is the process flow developed by Dave Huber (former Elegen PI) based on the nanoscribe document suggestions.

  - Remove the ITO Meso substrate from the encapsulating plastic.

  - Check which side has the ITO coating by measuring the resistance with the multimeter.  Only touch the probe towards the edge of the substrate, not in the center printing area.  You will want the ITO side facing up in the silanation bath.

  - Perform the standard substrate solvent clean – rinse with acetone, then methanol, then isopropyl alcohol and blow dry at the solvent bench.  Do not scrub with a wipe as suggested in the Nanoscribe protocol.  Place dry substrate ITO side up on a clean room wipe while preparing the silanation bath.

  - Prepare a beaker of silanizing solution - ~25 mL of acetone with 4 drops of silane solution (kept in the fridge).

  - Put the substrate in the solution with ITO side facing up, cover the beaker with parafilm  and incubate for at least two hours.  (Parafilm is used at Elegen offsite lab space.  It may be replaced by foil or cling wrap at SNF if needed).

  - Carefully remove substrate from the beaker and rinse in acetone, then methanol, then isopropyl alcohol over the drain to the solvent carboy.  Dry substrate with Nitrogen gun before mounting onto substrate holder for IP S resist drop casting.

- Amount and form:  Liquid sold in a 25 or 50 ml glass bottle.  If the bottle is too small for a yellow label we can put the small bottle in a secondary containment wide mouth bottle or jar.

- Storage: We would plan to store our bottle in the storage group L refrigerator for flammable materials.  Storage groupsstorage groups

- Disposal: The priming solvent solution will be disposed of by pouring into the solvent waste containment carboy at the bench where the processing will be done.  Dirty Au contaminated tweezers will be used to handle the substrate. Glassware and tweezers will be rinsed with acetone and isopropyl after use and allowed to air dry on the bench before transferring back to the storage cabinet across from FLEXCORR3 & 4. Aluminum foil, cling wrap or parafilm used to seal the beaker will be disposed of as solid solvent waste in a baggie with any contaminated wipes and disposed of in a red solid solvent waste can with the blue tag included for identification.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date:

V1.0