Request Title:  Use of AQUADAG E in Micromist coater

Requestor: Alexander Fieguth					Date:  12/04/18

Non-SNF staff, please complete the following:

Badger ID: afieguth

Company name/PI:  Giorgio Gratta

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material.

AQUADAG E also known as (BONDERITE S-FN AQUADAG E ACHESON) is a Water Based   Colloidal Graphite Resistance Coating. Containts Graphite (CAS: 7782-42-5) and (CAS: 1336-21-6). MSDS is attached.

- Vendor/manufacturer info:

Henkel Corporation

One Henkel Way

Rocky Hill, Connecticut 06067

(formerly produced by Acheson Industries)

Distributed for Acheson Colloids By: Ladd Research 83 Holly Court

Tel: (802) 658-4961

Fax: (802) 660-8859

e-mail: sales@laddresearch.com

- Reason for request: Conductive coating for various applications in high vacuum and potentially noble gases. Approximately very adhesive to different possible materials (as e.g. stainless steel, copper, gold) and also uniformly distributable. Micromist coater seems promising for the latter.

- Process Flow:  A premixed solution of the chemical diluted by water (1 part Aquadag to 5 parts water) and ammonium hydroxide to maintain pH~11 will be used. The substrate (copper, gold, stainless steal or similar) to coat will be cleaned using Acetone and will be heated by a hot plate (if possible). AQUADAQ will be then coated on the substrate using the Micromist coater.

- Amount and form. A small bottle with a few mL will be brought in and only the necessary amount to test the coverage on the substrate will be used. The bottle will be tagged and taken back after usage.

- Storage:  No storage needed.

- Disposal: No excess expected in Micromist coater. Remnants will be cleaned off and the nozzle as well as the syringe in contact with AQUADAG will be collected in a tagged bag and prepared for local waste collection.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: