Request Title:  HD Microsystems HD-8930, PI-2610, PI-2545 polyimide precursors and VM-651 adhesion promoter

Requestor: Henry Pang, Fardad Hashemi					Date: 03/27/2019

Non-SNF staff, please complete the following:

Badger ID: hpang@nikonrca.com, fhashemi@nikonrca.com

Company name/PI: Nikon Research Corporation of America

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. Please provide all common names, trade names, and CAS numbers where appropriate. Include an MSDS, if available; or provide the reason, if not. Make sure to include information for any new secondary chemicals (such as a developer for a new resist). Read the MSDSs as well as the Stanford Chemical Storage Groups and the Stanford Chemical Safety Data Base sections on this website to determine the Storage Group Identifier and Main Hazard Class of your chemical/material.

  - HD-8930 photosensitive polyimide precursor

  - PI-2610 non-photosensitive polyimide precursor

  - PI-2545 non-photosensitive polyimide precursor, wet etch compatible

  - VM-651 adhesion promoter for PI-2610 and PI-2545 non-photosensitive polyimide precursor

- Vendor/manufacturer info: address and phone number, website URL.

HD MicroSystems (http://www.hdmicrosystems.com/)

Address: 250 Cheesequake Road, Parlin, NJ, 08859

Tel: 1-800-346-5656

- Reason for request: Please give serious thought to this. If you have any process information (application notes from the vendor, protocol from another lab, experimental methods section of an article), please include it, preferably as attachments. Ask yourself these questions: Is this the latest procedure? Are there newer/safer alternatives that will also work for my project? Will any of the current SNF approved chemicals and materials work for me?

I plan to produce and pattern polyimide films that would be used as support and electrical insulation layers. To the best of my knowledge, SNF does not readily stock polyimide precursors that I require for my process flow. Therefore, I would like to bring in precursors newly purchased from the manufacturer. I will base my process flow according to the manufacturer’s official and most up-to-date process guides.

- Process Flow: Please provide a detailed process flow description on how and where you proposed to use this chemical. This should include all Lab equipment to be used for processing your wafers once your new chemical or material has been used (even if your new material is a film that is removed, it may still pose potential contamination concerns.) Make sure to include wet benches. Please note that if the chemical/material is to be used in any the "clean" equipment, purity specifications will be needed. This is most important for chemicals/material that are not normally used for VLSI device fabrication. To be allowed into a "clean" tool, the material should MOS grade or better.

Process flow for HD-8930:

  - Clean the substrate.

  - Spin coat HD-8930 polyimide precursor on the Headway Manual Resist Spinner.

  - Soft bake at 120oC for 180 seconds on a hot plate.

  - Expose the baked polyimide precursor using the Heidelberg MLA 150 or Karl Suss.

  - Develop the exposed polyimide precursor with TMAH-based developer (such as MF-26A) manually at wbmiscres or the SVG develop track.

  - Cure the polyimide precursor at 200oC for an hour at the Blue M Oven.

Process flow for PI-2610

  - Clean the substrate.

  - Spin coat VM-651 adhesion promoter on the Headway Manual Resist Spinner.

  - Spin coat PI-2610 polyimide precursor on the Headway Manual Resist Spinner.

  - Soft bake at 90oC for 90 seconds on a hot plate.

  - Cure the polyimide precursor at 250oC for two hours at the Blue M Oven.

Process flow for PI-2545

  - Clean the substrate.

  - Spin coat VM-651 adhesion promoter on the Headway Manual Resist Spinner.

  - Spin coat PI-2545 polyimide precursor using the Headway Manual Resist Spinner.

  - Soft bake at 140oC for 180 seconds on a hot plate.

  - Spin coat SPR-3612 resist using either SVG Coat Track or Headway Manual Resist Spinner.

  - Expose the soft-baked resist using the Heidelberg MLA 150 or Karl Suss.

  - Develop the resist and polyimide precursor together with TMAH-based developer (such as MF-26A) manually at wbmiscres or the SVG develop track.

  - Strip the resist at wet bench (wbflexcorr-3-and-4).

  - Cure the polyimide precursor at 250oC for two hours at the Blue M Oven.

- Amount and form. How much will you bring in? Is it solid, powder or liquid? (Note: as a general rule, powders are not permitted in the cleanroom.) Do you need to mix it to use it?

HD-8930 polyimide precursor: 4mL single-use bottle, liquid

PI-2610 polyimide precursor: 4mL single-use bottle, liquid

PI-2545 polyimide precursor: 4mL single-use bottle, liquid

VM-651 adhesion promoter: 4mL dropper bottle, liquid, dilute to 0.1% in DI water

- Storage: Will you be storing your chemical/material at SNF? If so, please note any potential reactivity’s (this should be on the MSDS). Storage groups A, B, D and L are stored in the yellow solvent cabinet in the furnace support area, while storage groups C, E, F and G are stored on top of one of the Pass-through Carts. Ensure your chemical container or material is properly labeled. If there is no available room, it must be stored by in the bulk storage area. You will then need to obtain it from receiving area personnel each time you want to use it and return it to them when you are finished using it (or each time you leave the lab). Note that there is no storage of chemicals/materials in the processing lab or at any wet bench.

No. I will bring the 4ml bottles into the facility each time. The bottles are disposed after use.

- Disposal: How will you dispose of any waste or excess chemical or material? In your discussions with experts and vendors, try to determine the best way to dispose of your spent chemicals and by-products. Please refer to the SNF Lab members Safety Manual for the different methods of waste disposal that are available in the lab.

All polyimide precursors would be consumed after the deposition/spin coat process. I will dispose the emptied bottles in the designated waste bottle bin, and dispose any unused diluted VM-651/DI water mixture into the designated solvent waste drain.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: