Request Title:  	CMP Polishing of Silicon Carbide in POLI-400L using specialized pad

Requestor: 	Daniil Lukin						Date:  April 2, 2019

Non-SNF staff, please complete the following:

Badger ID:	dlukin

Company name/PI:  Jelena Vuckovic

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. . The SiC-specific slurries are: ULTRA-SOL STD0.5μ20MCH and ULTRA-SOL STD3μ100M. The MSDS provided by Eminess were provided in a previously approved PROM request, dated September 12, 2018, and are attached again for reference.

- Vendor/manufacturer info: eminess.com

- Reason for request: Diamond slurry is not compatible with the IC1000 pads provided by SNF, and silica slurry is too soft to planarize the SiC after the previous grinding fab step.

- Process Flow: 
Sample pre-processing: Bond 5 SiC 1x1cm chips to a Si wafer with 3um thermal SiO2. The strength of SiC-SiO2 bond has been verified and exceeds material strength of SiO2. Use Disco grinder to thin down the SiC to below 5um. Clean group, but do not need to remain clean.
POLI-400L preparation (to be done by/under supervision of SNF staff): Remove IC1000 pad from a platen and dispose of the pad. Place a fresh SUBA 800 pad (purchased from Eminess, optimized for our slurry). 
Sample processing: Process our wafers in the CMP, first with coarse and then with fine Diamond slurry.
POLI-400L post-processing (to be done by/under supervision of SNF staff): Remove SUBA 800 pad and dispose of it. Place a fresh IC1000 pad (I already purchased one for this purpose) onto the platen.

- Amount and form. N/A

- Storage: Storage of platens and slurries is not in SNF.

- Disposal: The polishing pads can be disposed of into the general sharps or waste container. The Diamond slurry is compatible with the in-house slurries for disposal, as has already been determined in the previously-referenced PROM request.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: