Request Title: Request approve of negative photoresist ‘NR9-3000PY’ in SNF.

Requestor: 	Ji Won Seo			Date:  2019/05/20

Non-SNF staff, please complete the following:

Badger ID:	jwonseo@stanford.edu

Company name/PI:  Stanford university / Tom Soh

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material.  Negative photoresist NR9-3000PY, I attach the MSDS of the chemical in email.

- Vendor/manufacturer info: Futurrex Inc.,

Address: Corporate Headquarters, 24 Munsonhurst Road, Franklin, NJ 07416, USA

Phone number: 888-999-4188

Website URL: https://futurrex.com/en

- Reason for request: Firstly, I attach the protocol of NR9-3000PY, latest version.

When I was in my previous lab, We always used the NR9 for negative photoresist. It was very common negative photoresist.

The negative photoresist acted as a lift off sacrificial layer for metal pattern.

In SNF, there is a AZ5214IR  negative photoresist. However, the AZ5214 have very poor resolution and complicated process for patterning.

Moreover, there is a lol and lor series in SNF for lift-off process. However, they have too thin thickness of film and are not easy to be patterned by Karlsuss mask aligner.

Those are the reason for request this NR9-3000PY negative photoresist.

Moreover, there was already same photoresist with yellow label that someone is using in SNF. I attach the image of the bottle written same photoresist(NR9-3000PY). Someone already have been using it in SNF.

- Process Flow:

  - 4 inch Si wafer is spin-coated using Headway 2, soft bake 150c for 1 min 30 s in hot plate near the Headway 2.

  - Exposure using Karlsuss and my mask for 20s

  - Post exposure bake, 115c for 1min

  - Development using Developer MF26A for 30s in wbmiscres developer bench.

  - After process, the NR9 photoresist can be removed by remover PG or acetone for 1min.

- Amount and form. One 16 oz. bottle. It is liquid.  I don’t need to mix it to use it.

- Storage: I will store my chemical at SNF. terial at SNF? Storage groups is L

- Disposal: The waste during spin-coating will be in zip-rock bag and disposed in resist-waste trash can.   Unused product is a RCRA hazardous waste with numbers U057 and D001.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: